## Slide 1
Tom Connolly 1 Pavel Kurilovich 2
Spencer Diamond 3
Recovery dynamics of a gap-engineered
3D aluminum transmon after a quasiparticle burst
Heekun Nho
1. Google Quantum AI
2. Department of Physics, Harvard University
3. Northrop Grumman
4. Department of Applied Physics, Stanford University
5. Department of Physics, U.C. Santa Barbara
Acknowledgements:
Charlotte Bøttcher 4
Luigi Frunzio
Leonid Glazman
Michel Devoret 1,5
Department of Applied Physics, Yale University
current affiliations:
Notes: Going to tell you about how we can use the tools of single photon gen and detection
Presented by shyam in previous talk to realize concurrent remote entanglement
This is an essential primitive in quantum information, especially for modular architectures

## Slide 2
Nonequilibrium quasiparticles in superconducting qubits
DOS
observed “non-equilibrium” QP density
high energy phonons/photons
qubit state
past attempts of gap engineering with heterostructure:
Joyez et al. (1994), Lang et al. (2003), Sun et al. (2012), Riwar et al. (2016)
tunneling QP can relax or excite the qubit
rate of QP tunneling with
qubit transition
:
Can we reduce regardless of
by suppressing per- rate ()?

## Slide 3
Reducing QP-induced relaxation rate
using superconducting gap asymmetry near JJ
gap engineering with aluminum film thicknesses
Supercon. gap difference at JJ reduces QP-induced relaxation when
DOS
qubit state
Court et al. (2007)
Cherney et al. (1969)
Connolly&Kurilovich et al. (2024)
see also:
McEwen & Miao et al. (2024)
Diamond et al. (2022),
Pan et al. (2022)
Marchegiani et al. (2022),
Harrington et al. (2024),
10

## Slide 4
tune with JJ film thicknesses
( )
QPs thermalize to cryostat temperature
(when )
Connolly & Kurilovich et al. (2024)
Diamond et al. (2022)
Can gap engineering suppress the qubit decoherence due to high-energy impacts?
Reducing QP-induced relaxation rate
using superconducting gap asymmetry near JJ
gap engineering with aluminum film thicknesses
Here: steady-state

## Slide 5
(when )
Reducing QP-induced relaxation rate
using superconducting gap asymmetry near JJ
gap engineering with aluminum film thicknesses
Can gap engineering suppress QP tunneling even after high-energy impacts?
Impact of ionizing radiation deposits energy on substrate, resulting strongly out-of-equilibrium QP density and temperature
How fast do qubit/QPs/phonon bath recover?
Fowler et al. (2024)

## Slide 6
Controlling gap difference with film thickness
 | big- device | small- device
film thickness |  | 
film thickness |  | 
“big” device
“small” device
JJ
Al
JJ
Al
Al covers only 2% of chip area
measuring with steady-state QP density
sapphire

## Slide 7
Detecting QP burst events in transmons
no burst
burst
burst starts
QP burst observed in gap engineered device
big- device
reset to
reset to
reset to
pulse sequence for
burst detection:

## Slide 8
Detecting QP burst events in transmons
reset to
reset to
reset to
Caution:
1) detect only temporally-correlated errors
2) post-selection due to readout
pulse sequence for
burst detection:
(5% of events*)
no shift
(95% of events*)
*measured in 3rd device (Suppl. III.D)
sapphire

## Slide 9
Large modestly reduces burst occurrence
device |  | detected burst rate
big- |  | 
small- |  | 
device |  | detected burst rate
5x suppression
in detected event rate
If , suppression
steady-state
burst
burst threshold
calculated
QPs are hot during bursts?
non-exp.
initial decay
()
averaged over all detected events

## Slide 10
reset to
reset to
reset to
feedback measurement  extract only
repeated readout  extract
during QP bursts,
Qubit temperature as a proxy for
(hard to detect burst events when
qubit mostly stays in )

## Slide 11
single-shot joint parity-qubit state readout
e.g. during burst event (1 ms)
Parity-switching burst detection in big- device
collect more (weaker) burst events than thresholding on qubit relaxation events
 only changes scaling (Suppl. III.E)
cannot threshold on number of qubit transitions
device | qubit relax. burst rate | parity sw. burst rate
big- |  | 
small- |  | 
device | qubit relax. burst rate | parity sw. burst rate
Here: big- device
spike in both
qubit decoherence & parity-switching rate
parity sw. burst

## Slide 12
Recovery dynamics after QP bursts
burst QP density decays exponentially ()
Debye model predicts for in our chip
Here: big- device
non-exp. initial decay
()
(decoherence dominated by dielectric loss)
assuming during bursts,
decoherence rate decays within
see also:
Kurilovich & Roberts et al. (2026)

## Slide 13
Recovery dynamics after QP bursts
burst QP density decays exponentially ()
Here: big- device
(decoherence dominated by dielectric loss)
Phonons with can only escape through two clamps
e-h pairs
sapphire
phonons stuck in the chip and heat up the qubit/QPs
non-exp. initial decay
()
decoherence rate decays within
Debye model predicts for in our chip

## Slide 14
Recovery dynamics after QP bursts
burst QP density decays exponentially ()
Here: big- device
(decoherence dominated by dielectric loss)
non-exp. initial decay
()
decoherence rate decays within
Debye model predicts for in our chip
Cu phonon trap experiment:
Henriques et al. (2019), Iaia et al. (2022), Larson et al. (2025)
Small patch of Cu film ()
can absorb at

## Slide 15: Summary
Gap engineering is useful for mitigating QP bursts,
but its effectiveness is limited by temperature
How to suppress QP bursts further:
1. Increase gap difference above (e.g. gr-Al film)
2. Enhance phonon escape:
better thermalization/normal metal traps

## Slide 20
Debye model
  For our sapphire chip ,
Cu
  For patch,