## Slide 1: Measuring and Modeling the Impact of Radiation on Gap-Engineered Superconducting Qubits
Radiation Impacts on Superconducting Qubits 2026 June 16th, 2026
H.D. Pinckney1,2, P.M. Harrington1, K. Azar1, H.P. Binney1,2, A. Goswami1, M. Hays1, M. Moes7, J. Yang2, W. Van De Pontseele2,
F. Contipelli3, R. DePencier Piñero3, H. Stickler3, M. Randeria3, T. McJunkin4, A.W. Hunt4, Y. Jones-Alberty4, K. Schultz4,
B.M. Niedzielski3, M. Gingras3, M.E. Schwartz3, J.L. Yoder3, J.A. Grover1, K. Serniak1,3, J.A. Formaggio2,5, W.D. Oliver1,5,6
1Research Laboratory of Electronics, MIT 2Laboratory for Nuclear Science, MIT 3MIT Lincoln Laboratory 4Johns Hopkins Applied Physics Laboratory 5Department of Physics, MIT 6Department of Electrical Engineering and Computer Science, MIT 7Swiss Federal Institute of Technology ETH Zurich
http://arxiv.org/abs/2603.13460

## Slide 2: Radiation Mitigation: Gap Engineering
Ionizing radiation correlated errors
Substrate
Superconductor
…
Ballistic Phonons
Quasiparticles
(QP)
Cooper
Pairs
Vepsäläinen et al. (2020)
Wilen et al. (2021)
McEwen et al. (2022)
Harrington et al. (2024)
Bratrud et al. (2024)
Larson et al. (2025)

## Slide 3: Radiation Mitigation: Gap Engineering
Ionizing radiation correlated errors
Josephson junction gap engineering (JJ-GE) can suppress these errors
Aumentado et al. (2004)
Kamenov et al. (2023)
McEwen et al. (2024)
Nho et al. (2025)
Vepsäläinen et al. (2020)
Wilen et al. (2021)
McEwen et al. (2022)
Harrington et al. (2024)
Bratrud et al. (2024)
Larson et al. (2025)
Marchegiani et al. (2022)

## Slide 4: Radiation Mitigation: Gap Engineering
qb
JJ
0
1
Ionizing radiation correlated errors
Josephson junction gap engineering (JJ-GE) can suppress these errors
Aumentado et al. (2004)
Kamenov et al. (2023)
McEwen et al. (2024)
Nho et al. (2025)
Vepsäläinen et al. (2020)
Wilen et al. (2021)
McEwen et al. (2022)
Harrington et al. (2024)
Bratrud et al. (2024)
Larson et al. (2025)
Marchegiani et al. (2022)

## Slide 5: Radiation Mitigation: Gap Engineering
qb
JJ
X
0
1
X
Ionizing radiation correlated errors
Josephson junction gap engineering (JJ-GE) can suppress these errors
  Engineer such that JJ >
Aumentado et al. (2004)
Kamenov et al. (2023)
McEwen et al. (2024)
Nho et al. (2025)
Vepsäläinen et al. (2020)
Wilen et al. (2021)
McEwen et al. (2022)
Harrington et al. (2024)
Bratrud et al. (2024)
Larson et al. (2025)
Marchegiani et al. (2022)

## Slide 6: Radiation Mitigation: Gap Engineering
qb
JJ
X
0
1
X
Ionizing radiation correlated errors
Josephson junction gap engineering (JJ-GE) can suppress these errors
  Engineer such that JJ >
  Protects against “cold” QP on the low-gap side of the JJ
Vepsäläinen et al. (2020)
Wilen et al. (2021)
McEwen et al. (2022)
Harrington et al. (2024)
Aumentado et al. (2004)
Kamenov et al. (2023)
Bratrud et al. (2024)
Larson et al. (2025)
McEwen et al. (2024)
Nho et al. (2025)
Marchegiani et al. (2022)
McEwen et al. (2024)

## Slide 7: Radiation Affects Superconducting Qubits
Low rate of correlated errors remains
Google Quantum AI and Collaborators (2024)
Google Quantum AI and Collaborators (2024)

## Slide 8: Radiation Affects Superconducting Qubits
Low rate of correlated errors remains
  Consistent with cosmic ray protons and neutrons
Google Quantum AI and Collaborators (2024)
Fowler et al. (2024)
~ 1 impact/hour above 1 MeV

## Slide 9: Radiation Affects Superconducting Qubits
Low rate of correlated errors remains
  Consistent with cosmic ray protons and neutrons
Questions: to what degree does JJ-GE protect SC qubits? What about other GE strategies?
Google Quantum AI and Collaborators (2024)
Fowler et al. (2024)
~ 1 impact/hour above 1 MeV

## Slide 10: Radiation Affects Superconducting Qubits
Low rate of correlated errors remains
  Consistent with cosmic ray protons and neutrons
Questions: to what degree does JJ-GE protect SC qubits? What about other GE strategies?
Measurements:
  At MIT with 241Am
Collimator, ~100 m
241Am
JJ-GE Qubit

## Slide 11: Radiation Affects Superconducting Qubits
Low rate of correlated errors remains
  Consistent with cosmic ray protons and neutrons
Questions: to what degree does JJ-GE protect SC qubits? What about other GE strategies?
Measurements:
  At MIT with 241Am
  At APL with CLIQUE, a linear accelerator

## Slide 12: Three Devices Under Test
 | JJ [GHz] | M1 [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
Junction barrier
JJ
gnd
Junction Blocking Only
Junction Blocking and Ground Trapping
No JJ blocking
Profile of
JJ
JJ
gnd
gnd

## Slide 13: Three Devices Under Test
 | JJ [GHz] | M1 [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
Junction barrier
JJ
gnd
Junction Blocking Only
Junction Blocking and Ground Trapping
No JJ GE
Profile of
JJ
gnd
JJ
M1

## Slide 14: Three Devices Under Test
JJ Only
Junction Blocking and Ground Trapping
No JJ GE
Profile of
JJ
gnd
 | JJ [GHz] | M1 [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
Junction barrier
JJ
M1
JJ
M1

## Slide 15: Three Devices Under Test
JJ Only
JJ & M1
No JJ GE
Profile of
 | JJ [GHz] | M1 [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
JJ & M1
JJ
Junction barrier
JJ
M1
JJ
M1

## Slide 16: Three Devices Under Test
Junction barrier
JJ
JJ Only
JJ & M1
No JJ GE
Profile of
JJ
JJ
M1
 | JJ [GHz] | M1 [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ GE | 2.8 | 0.2 | 160 | 30
JJ Only | 10.0 | 0.1 | 200 | 10
JJ & M1 | 7.0 | 3.0 | 30 | 10
M1
M1

## Slide 17: Three Devices Under Test
Same mask design as Harrington et al. (2024):
  Qubit frequencies: 4-5 GHz
  T1’s ~ 20-50 s, readout fidelities ~90%
 | JJ [GHz] | gnd [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ blocking | 2.8 | 0.2 | 160 | 30
JJ blocking only | 10.0 | 0.1 | 200 | 10
JJ blocking and ground trapping | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ blocking | 2.8 | 0.2 | 160 | 30
JJ blocking only | 10.0 | 0.1 | 200 | 10
JJ blocking and ground trapping | 7.0 | 3.0 | 30 | 10

## Slide 18: Three Devices Under Test
Same mask design as Harrington et al. (2024):
  Qubit frequencies: 4-5 GHz
  T1’s ~ 20-50 s, readout fidelities ~90%
  Junction orientation dependence
 | JJ [GHz] | gnd [GHz] | SE Thick [nm] | SE Thin [nm]
No JJ blocking | 2.8 | 0.2 | 160 | 30
JJ blocking only | 10.0 | 0.1 | 200 | 10
JJ blocking and ground trapping | 7.0 | 3.0 | 30 | 10
 |  |  | SE Thick [nm] | SE Thin [nm]
No JJ blocking | 2.8 | 0.2 | 160 | 30
JJ blocking only | 10.0 | 0.1 | 200 | 10
JJ blocking and ground trapping | 7.0 | 3.0 | 30 | 10
S
S
S
F
F

## Slide 19: Tests with 241Am
A test source: 241Am
  5.5 MeV alpha (and 59 keV gamma)
Fowler et al. (2024)
~ 1 impact/hour above 1 MeV

## Slide 20: Tests with 241Am
A test source: 241Am
  5.5 MeV alpha (and 59 keV gamma)
  Expect 1 event per 13 seconds
  Measured on “JJ Only” and “JJ & M1”
Qubit error rate increased by alphas
  Observed rate matches expectation
Conclusions: While JJ-GE substantially reduces errors, JJ-GE qubits remain sensitive to rare, high Edep cosmic rays
  Motivates investigating additional mitigation strategies
Collimator, ~100 m
241Am
JJ-GE Qubit

## Slide 21: Hypothesis: Hot QP Mediate These Errors
QPs have extra energy which can facilitate tunneling
qb
JJ
X
0
1
X

## Slide 22: Hypothesis: Hot QP Mediate These Errors
QP
qb
JJ
X
0
1
QPs have extra energy which can facilitate tunneling
Excitation/relaxation error rate
increases during an “event”
Nho et al. (2025)

## Slide 23: Tests at JHU APL
Cryostat in linear accelerator beamline
  Thinned vacuum can and thermal shields
McJunkin et al. (2026)
arXiv:2603.13124

## Slide 24: Tests at JHU APL
Cryostat in linear accelerator beamline
  Thinned vacuum can and thermal shields
e-
McJunkin et al. (2026)
arXiv:2603.13124

## Slide 25: Tests at JHU APL
Cryostat in linear accelerator beamline
  Thinned vacuum can and thermal shields
Pulse width ~4 s
Accelerated electrons are minimum ionizing (5-25 MeV)
  Mean electron number: 0 6.5 e-
  Mean energies: 0 942 keV
e-
McJunkin et al. (2026)
arXiv:2603.13124

## Slide 26: Energy Dependence
Linac averaging reveals errors at the lowest measured energy (0.3 e- ~ 100 keV)
Conclusion: low-energy radiation still affects JJ-GE qubits
  As other error mechanisms are reduced, qubit sensitivity to lower energy radiation may become apparent

## Slide 27: Differences Between Devices – Severity
145 to 435 keV
Errors on JJ&M1 are more severe initially

## Slide 28: Differences Between Devices – Severity
145 to 435 keV
Errors on JJ & M1 are more severe initially
Conclusion: The “magnitude” of gap-engineering at the JJ () matters
145 to 435 keV

## Slide 29: Differences Between Devices – Recovery Time
145 to 435 keV
Errors on JJ & M1 recover faster
Hypothesis: Gap-engineering at the M1 interface (M1) traps QP away from the JJ
145 to 435 keV

## Slide 30: Qubit Frequency Shifts
Increased QP density decreased qubit frequency
Estimated with Ramsey interferometry
QP density recovers faster for JJ & M1
Conclusion: Gap-engineering at the M1 interface (M1) traps QP away from the JJ
Catelani et al. (2011)
Kurilovich et al. (2025)
Antonenko et al. (2026)

## Slide 31: Differences Between Devices
Conclusion: Gap-engineering at the M1 interface (M1) traps QP away from the JJ
Average of
1-3 electrons

## Slide 32: QP Modeling Goal
Re-create key features of our data:
  Event severity
  Recovery timescale
  JJ Orientation dependence
  Qubit frequency shift
Not a fit

## Slide 33: The QP model
A modified, time-dynamic implementation of the model from Marchegiani and Catelani (2025)
M1L
M3
M2
M1R
JJ
M1
Notes: Outline slide

## Slide 34
A modified, time-dynamic implementation of the model from Marchegiani and Catelani (2025)
Account for gap engineering by splitting QP density on low-gap side of JJ into two energy bins: greater than and less than
M1L
M3
M2
M1R
The QP model
JJ
M1
Notes: Outline slide

## Slide 35: The QP model
A modified, time-dynamic implementation of the model from Marchegiani and Catelani (2025)
Account for gap engineering by splitting QP density on low-gap side of JJ into two energy bins: greater than and less than
Dynamics through a time-dependent temperature describing the phonon bath
QP trapping effects modeled as coupling to two additional QP densities accounting for the base metal
M1L
M3
M2
M1R
JJ
M1
Notes: Outline slide

## Slide 36: The Model Itself
Coupled equations for change in reduced QP density
M1L
M3
M2
M1R
Thermal Generation
Trapping
Recombination
Time-dependent temperature
JJ
M1

## Slide 37: The Model Itself
Coupled equations for change in reduced QP density
For JJ-adjacent densities: add qubit transitions, QP relaxation and excitation
  Trapping assumed subdominant in leads
Scale factors for qubit variation
M1L
M3
M2
M1R
JJ
M1

## Slide 38: Qualitative Agreement with Data
Qualitatively re-creates gap profile influence on:
  Event severity
  Recovery timescale
  Qubit frequency shift
Notes: Outline slide

## Slide 39: Qualitative Agreement with Data
For qubits across the array, in excitation and relaxation, simultaneously
Notes: Outline slide

## Slide 40: Limitations
Qubit response averaged across impacts over whole chip
0D model, so no diffusion
Transition rates and model only assume 2-states
Yelton et al. (2024)

## Slide 41: Summary and Future
Radiation still affects aluminum JJ-GE qubits down to the lowest measured energy
Gap engineering at the JJ and M1 interfaces both matter
The degree of JJ-GE matters ()
Qualitative agreement with model of QP dynamics
Explore other mitigation strategies
  QP traps
  Further increased gap engineering (, M1)
Summary
Future

## Slide 42: Acknowledgements
MIT Engineering Quantum Systems (EQuS)
William D. Oliver, Jeff Grover, Max Hays, Patrick Strohbeen, Joel Wang, Terry Orlando, Kyle Serniak, Chihiro Watanabe, Lenore Buck,
Simon Gustavsson (now at Google Quantum AI)
Postdocs: Aziza Almanakly, Réouven Assouly, Fabrizio Berritta, Farid Hassani Bijarbooneh, Jorge Marques, Doug Pinckney, Holly Stemp, Helin Zhang
PhD students: Vaishnavi Addala, Junyoung An, Lamia Ateshian, Kate Azar, William Banner, Cora Barrett, Frederike Brockmeyer, Shoumik Chowdhury, Gabriel Cutter, Andy Ding, Ben Helman, Kotaro Hida, Shantanu Jha, Om Joshi, Harry Kang, Gyunghun Kim, Junghyun Kim, Jonathan Knoll, Maggie Marte, Chris McNally, Miguel Moreira, Sarah Muschinske, David Pahl, Lukas Pahl, David Rower, Chia-Chin Tsai, Hung-Yu Tsao, Beatriz Yankelevich, Sameia Zaman
Undergraduates: Oswin Cervantes, Justin Chen, Catherine Lowe, Mati Yablon
Visiting Member: Mathis Moes, Sein Park, Daniel Rocha, Gabriele Rolleri, Alexander Rommens
Collaborators: Joe Formaggio, Kevin O’Brien (MIT); Ben Loer (PNNL)
Quantum-Enabled Computation Group, MIT-LL
Superconducting Qubits Team:
Group Leaders: Mollie Schwartz, Kyle Serniak, Steven Weber, Jonilyn Yoder
Team Leads: Luke Burkhart, Rabindra Das, Michael Gingras, Thomas Hazard, Cyrus Hirjibehedin, Bethany Niedzielski Huffman, Katrina Sliwa, Donna-Ruth Yost
Team: Mike Augeri, Kate Azar, Peter Baldo, Jeffrey Birenbaum, Logan Bishop Van Horn, Tristan Brown, Gregory Calusine, Glenn Carl, Felipe Contipelli, John Cummings, David Danza, Dan Davis, Renée DePencier Piñero, Steven Disseler, Bryce Fisher, Ben Freiman, Jeffrey Gertler, Kevin Grossklaus, Karen Harmon, Mike Hellstrom, Gerry Holland, Jennifer Hritz, Sokharom Huon, Andrew J. Kerman, David Kim, Jeff Knecht, Arthur Kurlej, Duncan Miller, Nathan Miller, Jovi Miloshi, Maddie Morocco, Kevin Obenland, Christopher O’Connell, Mallika Randeria, Matt Ricci, Lila Rodgers, Robert Rood, Gabriel Samach, Meghan Schuldt, Arjan Sevi, Marcus Sherwin, Hannah Stickler, Chris Thoummaraj, Kunal Tiwari, David Volfson, Terry Weir, Zally Yun
Visiting Member: Serra Erdamar
Alan Hunt
Yenuel Jones-Alberty
Tom McJunkin
Kevin Schultz
Formaggio Radqb Group
Johns Hopkins Applied Physics Lab
Joe Formaggio, Doug Pinckney, Hannah Binney, Mingyu Li, Jiatong Yang