## Slide 1
Matt Pyle
UC Berkeley
RISQ 2026 @UW
Using Classical Superconducting Athermal Phonon Sensors to Understand Non-ionizing Backgrounds in Superconducting Qubits

## Slide 2: TES based Athermal Phonon Detectors
TES (W)
Athermal Phonon
Collection Fins (Al)
Substrate (Si, Al2O3)
1 cm
1 cm
R
T
Bandgap engineering is used to collect and concentrate QP to maximize sensing efficiency rather than to minimize sensitivity as in computational qubits

## Slide 3: Mysterious Phonon Burst Background (LEE)
CRESST III
2207.09375
CRESSTIII Background Studies
Expected Radiogenic Backgrounds
?
Si 0.35g
LiAlO2 11g
Al2O3 16g
Al2O3 16g
CaWO4 24g
CaWO4 24g
1. What’s the source of this background?
2. How can we minimize it?

## Slide 4: Phonon Burst Rate variation with time and Thermal Cycling
1. Phonon Burst rate monotonically decreases with time since cooldown
2.Partial reset with thermal cycling
Seen in all calorimeters to various extent
CRESST III
2207.09375

## Slide 5: 3) Phonon Burst Excess is Non-Ionizing
Drifting of e/h pairs converts electrostatic potential energy into additional athermal phonon energy. A 20eV recoil with 1eh event would have a 20eV+35eV=55eV total phonon energy.
Also seen in EDELWEISS
K. Kennard EXCESS 26
SuperCDMS
Recoil Phonons
Luke Phonons
ΔV
20eV recoil,1e/h Er @0V = 20eV
@35V: 20eV+35eV=55eV

## Slide 6: Not Just In Athermal Phonon Detectors …

## Slide 7: QP burst relaxation background in single e- qubits
RF single e- transistor show QP burst rate that relaxes with time
Manilla et al (2102.00484)
Chip held with vacuum grease?

## Slide 8: Non-Ionizing Phonon Relaxation Backgrounds in Computational Qubits too
Charge parity flip rate background limited by phonon burst relaxation processes in Yelton et al (2503.09554v1)
Al ground plane rate much lower than Nb ground plane rate -> phonon bursts
Charge rates constants -> non-ionizing
Charge rates don’t see relaxation
Non-ionizing phonon relaxation bursts seen in all superconducting technologies … this is a shared problem!

## Slide 9: Fact Summary
 | Phonon Calorimeters | Qubits
1) Variation with time since cooldown (and/or time since fabrication) | Yes | Yes
2) rate resetting with thermal cycling | Yes | Yes
3) Non-Ionizing | Yes | Yes
These facts are incredibly restrictive!
Athermal Phonon Detectors and Qubits are sensitive to the same underlying phonon burst background sources

## Slide 10: Hypothesis: Stress Relaxation?
Detector
Detector
Detector under stress due to thermal contraction,manufacturing, etc.
Detector relaxes releasing phonon energy
arXiv:physics/0504151
Potential Source Hypotheses:
metals/insulating substrate
detector substrate/support structure interface
Surface states
Bulk defects
?

## Slide 11: Recap of Previous Results from TESSERACT (with commentary)

## Slide 12: Phonon Bursts from GE varnish
Glued Down with GE varnish
(High Stress)
Hanging (low stress)
2 orders of magnitude difference in rate between high stress (glued) and low stress (hanging) device
2208.02790
GE varnish (and rubber cement) significantly increase <38eV backgrounds

## Slide 13: LEE from Glued Detector/Support Interface … Completely Robust
Also seen with rubber cement (qualitatively worse) -> unpublished
We do TES Tc runs to confirm fabrication quality pretty regularly that we just glue down, all have this qualitative effect -> unpublished
But ….

## Slide 14: QP poisoning from Glue LEE Not Measureable in Qubits
In Yelton et al (2503.09554v1), QP tunneling from GE varnish glued and wirebond supported (PT off ) are identical! Glue QP poisoning is subdominant to other LEE like QP poisoning mechanisms
Wirebond Supported
2503.09554v1
2503.09554v1
GE varnish Glue Support

## Slide 15: How do we reconcile these somewhat conflicting observations?
LEE/non-ionizing phonon burst rate incredibly susceptible to gluing SOP:
  How much GE varnish over how much area?
    UW Plourde: 4 mm2 squares in the corner
    UCB Pyle: 100% coverage
  Curing SOP: vacuum?, heat?, etc?
QP poisoning flip rate not dominated by phonon bursts in the 1-10eV range
Retest following Britton’s gluing SOP?

## Slide 16: PT Environmental Vibration Causes QP bursts In Wirebond Supported devices
In Yelton et al (2503.09554v1), QP tunneling rates asymptote in devices held by wirebonds
If you turn the PT off, relaxation is visible … PT vibrations are making QP. Definitely not what we saw in the published result. Why not? Well …
Wirebond Supported
2503.09554v1

## Slide 17: Complex Environmental Vibration Dependence: Correlated T1 Errors from PT Vibrations
MIT (2603.16494) measured the correlated QUBIT decoherence rate for a hanging qubit array with no bandgap engineering and found PT vibrations caused QP poisoning in one fridge but not the other.
Leiden PT415
Leiden PT415
Blufors XLD PT425

## Slide 18: Wirebond Holding has Significant Environmental Vibration Susceptibility
In Pyle lab (Cryoconcepts PT415) @ UCB, hanging devices have:
  ~50% of the time no measureable vibration power.
  ~50%: some-to-significant vibrational noise
2603.17964
Vibration excitation studies confirm that we are exciting vibrational modes in the wirebond/detector mechanical system:
If loss mechanisms are linear:
Due to the dominance of 2nd vibrational harmonic, we have a primarily linear system
really high quality factor: Q ~ 104
Sometimes your environmental vibrations overlap with the resonance sometimes they don’t

## Slide 19: Phonon Bursts from Vibrations
In most recent paper (2603.17964), the control device had very large transient coupling.
When vibrations are worst:
  Standard athermal phonon losses in foot
  eV (1014Hz) scale phonon bursts seen when vibrational power is highest!
2603.17964
2603.17964
For this run, a hard cut on DC parasitic power (baseline cut) removes all background rate – vibration phase correlation with 80% livetime.
Vibration PB subdominant above 5eV and the ROI was 15-30eV
even so, we likely wouldn’t have published if vibration LEE was on fast neutron exposed detector

## Slide 20: Best Structural Support?
Clamp
Hanging (low stress)
Resting
Glue
We’re many orders of magnitude away from where we want to be in Phonon Bursts. Thus, every source that is localized needs to be suppressed by many orders of magnitude.
Every DM experiment (and superconducting quantum computer?) needs a good vibration decoupler (as the CRESST/CUORE ecosystem knows)

## Slide 21: Phonon Burst Source: Substrate or Metal ?
We (and CRESST 2404.02607) see both shared and single channel relaxation events
Singles: Al metal film relaxation
Shared: Substrate Phonons
1% 2 Channel Device
2410.16510
R Romani

## Slide 22: Not Just In Athermal Phonon Detectors …

## Slide 23: Phonon Bursts in Far IR Resonator (MKID) Sensor Arrays
JPL (Day et al 2404.10246)
Standard single/shared topology of dark count rate in Far IR resonator sensor arrays
MKID Inductor Geometry

## Slide 24: Source of Shared Phonon Bursts ?
Test hypotheses with different substrate geometries
 | Scale with thickness | Independent of thickness
Scale with Aspect ratio | Substrate side wall | 
Independent of Aspect ratio | Wirebond support (likely some weird power) Substrate volume | Substrate top/bottom face

## Slide 25: Shared Phonon Burst Rate
Shared LEE scales with thickness
2505.16092

## Slide 26: Source of shared Phonon Bursts not the top/bottom polished face
 | Scale with thickness | Independent of thickness
Scale with Aspect ratio A tinge sketchy | Substrate side wall | 
Independent of Aspect ratio | Wirebond support (likely some weird power) Substrate volume | Substrate top/bottom face

## Slide 27: Comparing PB rate in CPDs and 1cm2
76mm diameter x1mm thick
CPDs and 1cm2 have pretty much the same background rate/mass above 10eV
Different support: clamp vs wirebonds
Different sidewall/volume ratio
2505.16092

## Slide 28: Source of shared PB in the substrate volume? warning: not a clean A/B test
 | Scale with thickness | Independent of thickness
Scale with Aspect ratio A tinge sketchy | Substrate side wall | 
Independent of Aspect ratio | Wirebond support (likely some weird power) Substrate volume | Substrate top/bottom face

## Slide 29: Could Bulk PB be Lattice Defect Complexes from fast neutron interactions?

## Slide 30: Physics of Lattice Defect Generation
Lots of computational/theoretical effort has gone into modeling defect generation due to nuclear recoils
  Nordlund 2408.07518
  Jay 10.1109/TNS.2016.2628089
  And many others …
By ~0.3ps, the nuclear recoil (PKA) has hard scattered with secondary atoms (SKA) and generated lots of defects.
Jay 10.1109/TNS.2016.2628089
Jay
Jay 10.1109/TNS.2016.2628089
After this defects begin to interact
  I and V recombine and anneal away
  I and I, V and V combine to make more complex defects configurations
Since 1I, 1V and 2I can diffuse at 300K, these annealing process can continue to occur at long time scales
Is LEE just the tail of this process ?
SRIM
Jay 10.1109/TNS.2016.2628089

## Slide 31: A/B Test for Fast Neutron Defect PB
Irradiate one detector of a near identical pair with a fast neutron source at 300K
We tried to really irradiate the detectors ... 2 orders of magnitude more total non-ionizing recoil energy than expected from cosmic rays …
Warning: AmBe/DD much softer spectrum than Cosmic Ray Neutrons

## Slide 32: Background in Irradiated Device vs Control
Definitely see excess background in irradiated device
Spectral differences from our usual LEE background … higher energy
Not enough to be the dominate source of LEE. We see a ~x10 increase in 15-30eV background where we would expect ~x100
Weird: the excess background shape wasn’t the same

## Slide 33: Time dependence of Background
Irradiated device background decays away with time since cool down just like the control does (and all of our devices) … SEEMS REALLY LEE LIKE

## Slide 34: Response to 50K Partial Warmup
After cycling the detectors to 50K ,the excess background in the irradiated device largely disappeared (if only all PB behaved like this). Fast Neutron generated backgrounds is like/not like real PB

## Slide 35: Remeasure 2 months later
Background is still a bit elevated, but nothing like before. Suggests that fast neutron defects continue to anneal at 300K on month time scales?

## Slide 36: Summary
Non-ionizing Phonon Burst now seen in all superconducting devices (qubits, resonators, phonon sensors)
Enormous progress in understanding the source:
  Structural support / Environmental Vibration
  Differential contraction between substrate/superconducting films (singles)
  Some source in the substrate volume
Fast neutron lattice irradiation @300K produces long time scale lattice defect relaxation events @10mK
  Tantalizingly similar to standard non-ionizing LEE
  Naively, rate too small to be a dominant component of our background LEE ?
  More studies needed

## Slide 37: Resonators as a Tool to Understand Qubit Backgrounds
Quasiparticle poisoning due to mm blackbody leakage first understood with resonators in 1105.4642.
Every qubit setup uses something like the box-in-box architecture proposed here today.

## Slide 38: Resonators as a Tool to Understand Qubit Backgrounds II
0802.4457 mapped out the frequency shift of resonators due to TLS as a function of CPW geometry (participation ratio) and found that the majority of the TLS seemed to be on the sapphire surface and not in the bulk
Classical superconducting resonators are an extremely powerful tool to understand sources of decoherence in superconducting qubits

## Slide 39: Phonon Sensors as a Tool to Understand Qubit Backgrounds?
Phonon Sensors are a powerful tool to understand non-ionizing qubit backgrounds because they are:
designed to be maximally collect and measure athermal phonons
Easily provide phonon burst energy information

## Slide 40: Backup

## Slide 41: Substrate History

## Slide 42: Single Events in Photon Calibration too
Calibration photons have single and shared events too!
Shared = substrate absorption
Singles = Al fin absorption
1 Al fin photon + 1 substrate photon

## Slide 43: Single Relaxation Event Pulse Shape
Single LEE background source is Al film relaxation!
LEE single pulse shapes and Al fin calibrations photons have pulse shapes consistent with a dirac delta energy pulse that saturates a single phonon sensor in the channel
As LEE energy drops, pulse shape looks more like a dirac-delta energy deposition (known from dIdV)

## Slide 44: Perfect A/B Test?
For a systematically clean measurement of LEE dependence on thickness, we must keep all other variables identical
 | Same | Differences
Design | identical | 
Substrates | >20kOhm cm Intrinsic Si double side DSP | Different Boules Baking times slightly different
Fabrication | Same SOP Texas A&M fabrication facility | Consecutive fabrication runs separated by 1 week
Dicing | Same vendor | Different blade thickness
Storage, Shipping | Identical | 
Measurement | Same run/cooldown, nominally same electronics chain | Different vibration susceptibility