## Slide 1: Geometry Optimization and Distributed Coupling for High Gradient NCRF Structures
Sami Tantawi

## Slide 2
Outline
Physics of breakdown
in high gradient normal conducting structures
The distributed-coupling technology
New geometric optimization capabilities
Cryogenic-copper structures
New accelerating frontiers for high-gradient operation
Next-Generation Distributed-Coupling Linacs
Making full benefit of the optimization capability of this novel technology

## Slide 3: New Discovery of Magnetic Fields Role in Breakdown Triggered a Change in Research Direction
3
Geometrical Studies: Standing-wave structures with different iris diameters and shapes a/l=0.215, a/l=0.143, and a/l=0.105
Pulsed heating and crystal orientation: Annealed Copper with large grain shows crystal pattern because damage is different for each crystal orientation
Evidence of pulsed heating due to magnetic field triggers crystal plane slippage that caused breakdown due to electric filed
New research initiated
    Geometry optimizations for accelerator structures based on reduction of the magnetic surface field
    Studies of surface magnetic fields and materials
    Basic Physics studies with mixed E&H dual-mode cavities
    Low temperature experiments with very high gradient structures
Applications of new information
    A new methodology for designing Photonic Band Gap (PBG) structures
    New understanding of MUON cooling cavity results in operation under strong magnetic fields
    Improved design of high peak power rf sources
Valery Dolgashev et al., “Geometric dependence of radio-frequency breakdown in normal conducting accelerating structures,” Applied Physics Letters, Volume 97, Issue 17, pp 171501 - 171501-3, October 2010.
Alex Cahill et al., "High gradient experiments with X-band cryogenic copper accelerating cavities" Phys. Rev. Accel. Beams 21, 102002 – Published 23 October 2018.

## Slide 4
Optimized Geometries
using
Distributed-Coupling Topology

## Slide 5: Distributed coupling Linacs provides a new technology that enables much flexible cell-design optimization
Distributed-coupling linac
The existing linac designs requires careful consideration of the coupling between cells
which limits the ability of designers to optimize the cell shape.
The distributed coupling linac overcomes these limitations by providing a new topology
that allows feeding each accelerator cell independently using a periodic feeding network.
New Scaling Laws Determine the Best Performance for Accelerating Structures
Tantawi et al. “Distributed coupling and multi-frequency microwave accelerators,” Jul. 5 2016, US Patent 9,386,682.
S. Tantawi, M. Nasr et. al. "Design and demonstration of a distributed-coupling linear accelerator structure." Physical Review Accelerators and Beams 23.9 (2020): 092001.

## Slide 6
Novel Manufacturing Techniques

## Slide 7: Novel fabrication methods are compatible with hard metals and reduced cost
Milling structure out of two halves instead of machining and then brazing single cells
No RF currents through the joint
Consistent with manufacturing structures out of hard copper alloys
Developing new manufacturing techniques to implement advanced materials in practical accelerating structures and reduce costs
Demonstrated with Standing and Traveling Wave Structure
S. Tantawi, P. Borchard, Z. Li
V. Dolgashev
Notes: This technique have proved efficient operation in practical accelerators at high-gradient operation

## Slide 8: Distributed coupling Linacs provides a new technology that enables much flexible cell-design optimization
Tantawi et al. “Distributed coupling and multi-frequency microwave accelerators,” Jul. 5 2016, US Patent 9,386,682.
S. Tantawi, M. Nasr et. al. "Design and demonstration of a distributed-coupling linear accelerator structure." Physical Review Accelerators and Beams 23.9 (2020): 092001.
Designed to minimize surface magnetic field
-mode, X-band, 20 cells Linac
Easy tuning and single frequency rather than 20

## Slide 9
Cryogenic Operation
of
Normal Conducting Structures

## Slide 10: High-power test of the distributed-coupling structure (Xband, 20 cells) at LN cryogenic temperature (77k)
Modeled structure gradient confirmed with electron beam
Room Temp (300k)
Cryogenic Temp (77k)
Stepped pulse with flat gradient of 200ns
Reduced breakdown rates compared to 300k operation
Pixels
Beam Energy
84MeV
Gradient=145 MV/m
Measured
Simulated
M. Nasr et al. "Experimental demonstration of particle acceleration with normal conducting accelerating structure at cryogenic temperature." Physical Review Accelerators and Beams 24.9 (2021): 093201.

## Slide 11: High-power test of the distributed-coupling structure (Xband, 20 cells) at LN cryogenic temperature (77k)
Modeled structure gradient confirmed with electron beam
Reduced breakdown rates compared to 300k operation
Measured
Simulated
 | 300k | 77k
 | 1 | 2.25
 | 155 | 350
BDR |  | 
 | 300k | 77k
 | 1 | 2.25
 | 155 | 350
BDR |  | 
High RF-to-beam efficiency
Heavy beam loading
Cost-efficient solution with LN
Reduced breakdown rates
M. Nasr et al. "Experimental demonstration of particle acceleration with normal conducting accelerating structure at cryogenic temperature." Physical Review Accelerators and Beams 24.9 (2021): 093201.
Room Temp (300k)
Cryogenic Temp (77k)
Stepped pulse with flat gradient of 200ns

## Slide 12: Distributed coupling structures are indestructible.
structure had a field enhancement factor of 2.6.
Old distributed coupling structure, Suface deformation happened at 300 MV/m

## Slide 13
Next-Generation
Distributed-Coupling Linac

## Slide 14: Next-generation distributed coupling linac: New geometric-optimization approaches and optimized ports
New geometric-optimization approaches
The cavity curvature is defined with a set of control points with variable positions to control splines which describes the cavity shape.
M. Nasr et al. New Geometrical-Optimization Approach using Splines for Enhanced Accelerator Cavities’ Performance, IPAC’18
Beam Axis
M. Nasr, and S. Tantawi
The first design with circular shapes
Can we do better?
Notes: Successfully verifying the operation of the first distributed-coupling linac
We started developing the next generation of distributed-coupling linacs
Benifiting from the design flexibility of the distributed-coupling topology and overcoming the limitations of the first design

## Slide 15: Next-generation distributed coupling linac: New geometric-optimization approaches and optimized ports
Target: Maximize shunt impedance with peak surface E-field to gradient ratio of 2
New geometric-optimization approaches
(MV/m)
(MA/m)
Distance along the surface (cm)
Gradient=100MV/m
X-band, 11.424 GHz, iris diameter
Peak surface E-field to gradient reduction from 2.5 to 2
with even higher shunt impedance
a.u.
M. Nasr, Z. Li, and S. Tantawi
M. Nasr et al. New Geometrical-Optimization Approach using Splines for Enhanced Accelerator Cavities’ Performance, IPAC’18
Optimized coupling ports
Reducing magnetic field enhancement to from 2.3 to 1.17
H Field
Starting shape
Optimized shape

## Slide 16: Next-generation distributed coupling linac: New geometric-optimization approaches and optimized ports
New geometric-optimization approaches
Peak surface E-field to gradient reduction from 2.5 to 2
with even higher shunt impedance
M. Nasr et al. New Geometrical-Optimization Approach using Splines for Enhanced Accelerator Cavities’ Performance, IPAC’18
Optimized coupling ports
Reducing magnetic field enhancement to from 2.3 to 1.17
M. Nasr, Z. Li, G. Bowden, and S. Tantawi
Notes: We finalized the full structure design along with the mechanical design
, and we tested the manufacturing of our structure using a set of prototypes, and it is currently being built

## Slide 17: Having every cell fed individually by a manifold naturally inspires the use of another manifold with another mode feeding the same cell
Performance of cavity improves when powered with two different RF modes
Efficiency: Linear superposition of fields by adding power in the two modes.
Gradient: doubling the accelerating gradient without doubling surface fields
Power (gradient)2
Optimum designs require non-harmonic operation; instead, we design for frequencies that are not necessarily harmonically related, but rather have a common sub-harmonic.
S-band
C-band
 | 2.856
 | 6.664
 | 952
 | 155
 | 2.856
 | 6.664
 | 952
 | 155
M. Nasr, and S. Tantawi
M. Nasr et al. “A Novel Dual-Mode Dual-Frequency Linac Design”, IPAC’17
M. Nasr et al. “The Design and Construction of a Novel Dual-Mode Dual-Frequency Linac Design”, IPAC’18
Mode01
Mode02
Total
(a.u)
Energy gain(a.u)
Distance along the surface (cm)
Distance along the surface (cm)
Notes: Increasing the gradient for single-mode operation comes at the cost of a larger increase in the input power with a square relation
On the other hand, dual-mode operation increases the system efficiency by boosting the accelerating gradient with a linear superposition of the power from the two modes; which increases the system efficiency
Also, Generally, the peak fields for the two modes doesn’t add up simultaneously on the surface
We found that our optimum designs require….
Thus, our designs still support multi-bunch operation separated by multiples of the common sub-harmonic period of the operating frequencies.
Our dual-mode design operating at S and C bands achieves a shunt impedance that is compatible with the one for our X-band design, but with double the iris diameter
And as we can see, an electron beam traveling on-axis experience the acceleration from both modes

## Slide 18: Distributed coupling with smooth-wall waveguide distribution manifolds
The guided wavelength, , exceeds the free space wavelength, .
Each manifold needs to be tapped every where, typically,
Then, the phase difference between every cavity is either or zero for respectively.
For a given number of manifold, each feeding every cavity, the phase advance, is given by: ; where is an integer, and .
The guided wavelength is readily calculated as
This expression for the guided wavelength does not yield a until ; consequently, the natural minimum for the number of manifolds required is three.
0
0
0

## Slide 19: 135 degree phase advanced distributed coupling structure
If one includes the period as an optimization parameter then the optimal structure with the minimal surfac magnetic field, and consequently the highest shunt impedance occurs at ~ phase advance; a natural choice is phase advance.
Every 4th cavity has a phase shift, hence 4 manifolds are needed to feed the structure.
Every two manifolds need to be fed with a phase shift; naturally fed by a hybrid that isolates the forward signal from the reflected signal.
Marco Oriunno, J. Merrick, G. Bowden, Z. Li, C. Nantista, E. Snively, M Shumail, S. Tantawi

## Slide 20: 135 degree phase advanced distributed coupling structure
If one includes the period as an optimization parameter then the optimal structure with the minimal surfac magnetic field, and consequently the highest shunt impedance occurs at ~ phase advance; a natural choice is phase advance.
Every 4th cavity has a phase shift, hence 4 manifolds are needed to feed the structure.
Every two manifolds need to be fed with a phase shift; naturally fed by a hybrid that isolates the forward signal from the reflected signal.
Marco Oriunno, J. Merrick, G. Bowden, Z. Li, C. Nantista, E. Snively, M Shumail, S. Tantawi

## Slide 21: Dual Moded Distributed Coupling 3 Linac
Ultimate shunt impedance, bigger apertures without loss of efficiency.
The elimination of the spigot length compacted the structure horizontally. Hence, operation at low frequency would still yield a reasonably sized device, which would allow us to think about a superconducting implementation.
Electrically it is a standing wave accelerator. For the point view of the source it acts as travelling-wave accelerator.
The manifold provide damping for both dipole polarizations.

## Slide 22: Optimized Cavity for the 3π/4 phase advance linac

## Slide 23: Dual moded Manifold feeding a set of 16 cavities. Each mode feeds 8 cavities

## Slide 24: Single cavity-Manifold design optimized for a chain of 8 cavities (32 cavities total in the linac)

## Slide 25: dual-mode launcher

## Slide 26: Integrated Linac that comprise the cavities, manifolds and the mode launchers Structure termination

## Slide 27: Manifold termination topology
The last two cavities within a manifold are fed differently from the rest of the linac cavities.
The reflection coefficient for each mode within the manifold is synthesized to achieve a particular scattering matrix needed for the manifold termination.

## Slide 28
Understanding the physics of breakdowns triggered new research directions for high-gradient operation
Distributed-coupling technology enables much flexible cell-design optimization and pushes the limitation of Linacs performance.
Cryogenic-copper accelerating structures have the promise for a new frontier for beam brightness, efficiency and cost-capability
Conclusion

## Slide 29
Thanks!
Questions?