## Slide 1: Dielectrics for High Gradient Normal Conducting Structures
January 20, 2026
Alexei Kanareykin
On behalf of Euclid’s/AWA ANL’s team
GARD RF Roadmap - NCRF Meeting

## Slide 2
Outline
www.euclidtechlabs.com
Brief history of the DWA
Materials for the DWA structures
Structures designs and novel structures
Materials with extreme low losses
    DWA programs in the U.K, Japan and FACET
    Exotic materials for the DWA structures (diamond, ferroelectric and conductive ceramic)
    Summary

## Slide 3
Timeline of Dielectric Accelerators
Electric Field Vectors
DWA Geometry
Features:
Simple geometry.
Small transverse size.
Short rf pulse, high reprate, preferred.
1951
1958
30MV/m
1989
DWA
2000
D. TBA
2006
100MV/m
~GV/m
2007
2011
Tunable DLA
2016
Staging
400MeV/m
theory
1963
First electron linac at Stanford
(1947)
Short pulse
2018-2025
Notes: D

## Slide 4
Dielectric based accelerator advantages:
design simplicity: no tight tolerances – 2D structure
Ez field magnitude (γ>>1) is flat at cross-sections;
Short RF pulse X - Ka band,, high reprate
THz structures at ~ 0.5-1.0 GV/m gradient
diamond thermal conductivity
reduced BBU instability;
enables tuning;
…..
Why Dielectric Based Accelerator ?

## Slide 5
Materials for the Dielectric-Based Wakefield Accelerator
Quartz, ε~ 3.75, tanδ~10-4

## Slide 6
Dielectrics Tested as DWA Loading
THz experiments at FACET and ATF

## Slide 7
Loss Tangent and Dielectric Constant of Microwave Ceramic
tanδ ~ f [GHz] over a wide microwave frequency range. Q×f ≈ const, [GHz], Q=1/tanδ. The product of frequency and dielectric quality is a constant. This relation is a very important characteristic of linear microwave ceramics
Q × f ≈ const [GHz]
Best Q*f is in the range 150,000-180,000 (MgTi)
tanδ~5*10^-6 at X band (10 GHz)

## Slide 8: Survey of dielectric based structures

## Slide 9: Dielectric Disk Accelerator (DDA)
(a) dielectric-lined circular waveguide, and (b) dielectric disk-loaded circular waveguide.
A Dielectric Disk cell: a) geometry;
b) electric and
c) magnetic fields of the accelerating mode;
J. Shao et al. Proc. IPAC’18, p.640
.
a
ba
c

## Slide 10: DDA structure
Dielectric-disk accelerator
J. Shao, et al, in Proceedings of IPAC2018, (2018)
Clamped structure achieved 102 MV/m accelerating gradient from 320MW
input power.

## Slide 11
D. Satoh et al. NIM B 459, 148, 2019, references there in
Dielectrics with extreme low losses vs. permittivity

## Slide 12
D. Satoh, M. Yoshida, and N. Hayashizaki. PRAB, 20, 091302 (2017)

## Slide 13
D. Satoh et al. X-band dielectric assist accelerating structure. LCWS-2024
During the high-power test, blue luminescence was detected. → caused by impurities in the sapphire due to electron impacts from multipactors.
•

## Slide 14
Dielectric Assist Accelerating (DDA) Structure at Cryogenic
D. Satoh et al. NIM B 459, 148, 2019.
D. Satoh et al. investigated the (2D) DAA structure operating at a cryogenic temperature. A simulation of a five-cell C-band (5.712 GHz) DAA structure with a BMT-BMW ceramic indicated that Q0 of the accelerating mode was over 120,000 and Zsh exceeded 850 MΩ/m at room temperature.
For the DAA structure operating at a cryogenic temperature of 27K, Q0 and Zsh of the DAA structure, high-purity MgO were to be greater than Q0= 765,000 and Zsh= 3.8 GΩ/m, respectively.

## Slide 15
DWA at CLARA, Daresbury, U.K.
Quartz – preferred material. Different thicknesses down to 25 microns for single mode tunable Cherenkov radiation generation.
For a wakefield streaker to measure ultra-short bunches from LWFA, a structure with 20micron thick Mica was fabricated. Mica: eps~ 6.4 to 9.3, loss tangent 10^-4 to 5x10^-3
The energy booster for the Compact Linear Accelerator for Research and Applications (CLARA) at Daresbury Laboratory is planned to be utilizing dielectric wakefield acceleration (DWA). Research is concentrated on the transverse wakefields limitations (BBU) instability, utilizing round or planar structures and elliptical beams.
Compact Linear Accelerator for Research and Applications (CLARA) , Daresbury Lab, U.K., 250 MeV, 250 nC, ~ ps range.
CLARA - 35 Mev, 100s fs 100 pC bunches
T.J. Overton et al. NIMA, 1072, 2025, 170160
silicate minerals, KAl₂(AlSi₃O₁₀)(OH)₂

## Slide 17
Relativistic, high intensity and small emittance electron bunches are the basis of linear collider and FEL projects. Using Cherenkov radiation generated by a high current bunch passing a dielectric wake-field accelerator may provide a significant cost saving and reduction of the accelerator facility size.
Advanced Acceleration for Future Linear Colliders
In collaboration with ANL/AWA
Euclid is developing critical components for two SWFA milestones:
0.5GeV demonstrator at Argonne National Laboratory
Collinear wakefield accelerator energy doubler.
Novel Dielectric Disk Accelerator, first time demonstrated 100MV/m, multipactor free.
Novel short pulse traveling wave photogun, record high gradient: 400MV/m, and insignificant dark current
0.5GeV Demonstrator

## Slide 19: Diamond
ε = 5.7; tan δ < 5∙10-5 at 30 - 145 GHz
High breakdown threshold (DC~2GV/m)
SEE reduction by surface dehydrogenation
High thermal conductivity = 25 W∙cm-1∙K-1 (5xCopper)
Hardness, low coefficient of friction
Low thermal expansion
Radiation resistant
~ 2 inch long
CVD diamond tubes ~20 GHz
Thin films for THz structures (manufacturing one unit for NIU)
Capillaries via CVD diamond (plasma capillaries for LBNL (funded by SBIR) and Oxford)
Euclid Techlabs experience:

## Slide 20: Diamond test at the AWA
Frequency | 24.81 GHz
Gradient (AWA 70 nC) | 60 MV/m
Beam gap | 4 mm
Diamond thickness | 1.2 mm
Structure width | 8 mm
Diamond length | 4 mm
Dielectric constant | 5.7; tan(δ) = 10-4
Q, quality factor | 2800, τ ~ 35ns
r/Q | 11.4 kΩ/m
Diamonds (E6) ...with a groove
Upper half of the diamond resonator
electron beam
Single crystal CVD diamond (E6)
Groove: 20um (wide) x 200um (deep)
Field enhancement ~ ε∙E ≈ 300 MV/m
AWA transported 72nC through the structure

## Slide 21: Conductive Low Loss Ceramic
Ceramics subject to DC electron beam for 2.5 hours
Conductive ceramic effectively discharges DC electron beam directly impinging on surface
Non-conductive
Conductive ceramic
30 sec
60 sec
90 sec
DC electron beam was deflected in 90 sec
21
tan δ at 650 MHz

## Slide 22
SUMMARY
Simple geometry, Small transverse size, Short rf pulse/high reprate preferred
Tested for 400 MV/m at X-band and Ka-band, > 1GeV/m at THz
Various materials with dielectric constant from 4.4 up to 50
Engineered materials with required RF properties (low loss ceramic)
Extreme low losses at cryogenic temperatures
New advanced materials to be tested (diamond, ferroelectrics, conductive ceramic)