## Slide 1: Engineered Nb surfaces
Potential and future R&D directions
Marc Wenskat (DESY)
5.2.2026 GARD RF Roadmap Update

## Slide 2: Can be split in two research topics
Surface passivation / encapsulation
Why do we care?
Various approaches & results
Outlook
Superconducting thin films
Reminder why/how it should work
Status & results
Outlook

## Slide 3: Surface passivation Surface encapsulation

## Slide 4: Experimental evidence: native oxide matters in itself I
and not indirect as e.g. source of oxygen
[Groll, N. R., et al. arXiv:1805.06359 (2018)]
[Proslier, T., et al. IEEE Transactions on Applied Superconductivity 21.3 (2011): 2619-2622]
[Kharitonov, M, et al. Physical Review B 86.2 (2012): 024514]
Cavity cut-outs identified by TMap
Hot Spots
Cold Spots

## Slide 5: Experimental evidence: native oxide matters in itself II
and not indirect as e.g. source of oxygen

## Slide 6: Experimental evidence: native oxide matters in itself III
and not indirect as e.g. source of oxygen
[Prudnikava, A. et al., SRF2025 TUA04]
Mid-T under vacuum twice and tested
→No/little oxide present
Stored under vacuum for 1.5 years
Leak caused pressure rise from 10-6mbar to 10-1mbar
Oxide regrowth added ~1.3 nΩ

## Slide 7: What do we know about Nb-oxides? It‘s complicated!
~5 nm
Off-stochiometric phase
Globaly, the ratio 2 Nb : 5 O is achieved
Locally, maybe Nb10O23 → O-depletion
Not vacancies in a lattice, simply bad matching
„Unbound binding electrons“ of Nb
Periodic Lattice
[Sheridan, Evan, et al., arXiv preprint arXiv:2111.11684 (2021)]
[Harrelson, Thomas, et al., arXiv preprint arXiv:2111.11590 (2021)]
[Murthy, Akshay A., et al. ACS nano 16.10 (2022): 17257-17262.]
[Herval, Leonilson KS, et al. Journal of Alloys and Compounds 653 (2015): 358-362.]
Reality:
Energetically not favored at RT, not “our” Nb2O5

## Slide 8: Same same, but different
Depending on the amplitude of the RF field the same microscopic state - unbound binding electrons - is used/interpreted/labeled differently, because different effects are dominant for the RF response
As both effects are caused by the same microscopic origin: if we study one, we might learn about the other
Eacc (number of photons)
low
high
Electron spins alignment (dangling bond) can be in two different configuration → Two-Level System
Application: Quantum computing
Magnetic moment of spin act as magnetic scattering site, causes pair breaking → Magnetic impurities
Application: Accelerators

## Slide 9: Currently four labs are conducting passivation studies
SQMS @ FNAL
  See previous talk by D. Bafia
  Encapsulation of cavities by CEA + subsequent annealings at FNAL
  Application quantum computing
CEA
  Atomic Layer Deposition of: Al2O3, Ta2O5, ZrO2
  Fundamental R&D, started with SIS studies
  Funding granted with QC application
Cornell
  Electroplating of Au
  Fundamental R&D
  Application is SRF
U Hamburg & DESY
  Atomic Layer Deposition of: Al2O3, Ta2O5
  Fundamental R&D, started with SIS studies
  Application is SRF & a little bit QC
[Grasslino, L. et al., SRF2025 THA04]
[Kalboussi, Y., et al. Applied Physics Letters 124.13 (2024)]
[Kalboussi, Y., et al. Physical Review Applied 23.4 (2025): 044023]
[Seddon-Stettler, S, et al. SRF2025 WEB07C]
[Méndez, Cristóbal, et al. arXiv preprint arXiv:2509.02914 (2025)]
[Wenskat, M, et al. SRF2023 TUIBA02]
[Rakshith, V. et al. SRF2025 TUP16]
10nm Al2O3 + 10h@650°C
1.5K
18nm Al2O3 + 3h@300°C

## Slide 10: Open questions, future & potential R&D
Two main directions: quantum computing and surface resistance tuning
  Synergy between both fields
    “same same, but different”
    leverage to attract young brains & resources
For SRF the interplay between oxide properties and consequences of removing it should be studied
  Can dissolve the native oxide only once → finite resource of interstitial oxygen
  Additional variable to tune annealing process parameters & protection against C-pollution(?)
“Optimal” material for encapsulation? Oxides? Which one? Au? Other?

## Slide 11: Superconducting thin films

## Slide 12: Differentiation wrt other talks
Here: Looking at R&D where „thinness“(d ≈ λL) of films is vital and not necessarily the material
Exclude R&D which use thin films (compared to cavity wall thickness) which replace bulk Nb
with another „bulkish“ (d>>λL) higher-Tc material
See talks in next session for that
Uttar Pudasaini (Jlab), Nathan Sitaraman (Cornell), Cristian Pira (INFN), Grigory Eremeev
Thin-Film Roadmap – report of European IFAST project
More to thin films than SIS

## Slide 13: Evolution of SIS Theory
The whole is more than the sum of ist parts
Energetically suppressed vortices in thin films cause enhancement of “field of first flux entry” a.k.a. Hc1
Alex’ idea: Coat a cavity with a thin superconducting film with insulating layer, acting as vortex barrier
Controversy around effectiveness
Taka’s new argument: Bean-Livingston Barrier increase through “counter current”
[G. Stejic et al., PRB 49.2 (1994)]
Co-Autor: Gurevich
[N. Schäfer et al., J. Appl. Phys. 128, 133902 (2020)]
Hc,1 of Nb3Sn is 50mT
[A. Gurevich, APL 88 (2006)]
[D. Liarte, SUST 30 (2017) 033002]
[T. Kubo, SUST 30 (2017)]
[Asaduzzaman, arXiv: 2304.09360]
[Keckert, S. PhD Thesis, Siegen 2019]
‘Pancake’ vortex

## Slide 14: By tuning layer thickness you increase Eacc and reduce Q0
Depends on Hc,1 and λL of both SC and “defectiveness” η
Optimization: what quenches first - substrate or layer?
  Thickness of insulating dI and sc film ds are free parameters
  Shifting B-field and current density j around
Realistic material parameters give you:
  Eacc ≈ 70-100 MV/m
  Q0 ≈ 3-5 x1010 (depends on Rres) @ 2K
This is all just on paper
[T. Kubo, SUST 30 (2017)]

## Slide 15: Who is conducting SIS research?
Coating:
  KEK used to, FNAL expressed interest
  Several labs work on planar samples (sputtering)
  CEA & U Hamburg work on cavities (ALD)
  …
R&D network much larger
  See Thin-Film Roadmap
Research – not just coating

## Slide 16: Method of choice: Atomic Layer Deposition
Achieves homogenous uniform coating on complex geometry with no shadowing effect
Taken from: L. Mai, (2020), DOI:10.13154/294-7658.

## Slide 17: Cavity results
Only two labs conduct cavity coating
18 nm Al2O3 on Nb
[Wenskat, M. et al 2023 Supercond. Sci. Technol. 36 015010 ]
50 nm NbTiN/ 7nm AlN on Nb + 900°C annealing
10 nm Al2O3 on Nb + 650°C for 4/10h
[Kalboussi, Y. et al SRF2023 WEIBA01]
[Kalboussi, Y., et al. Applied Physics Letters 124.13 (2024)]
[Y. Kalboussi. Nano hetero-structures for improving performances of superconductors under high fields. Université Paris-Saclay, 2023.
⟨NNT : 2023UPASP029⟩ ]

## Slide 18: Open questions, future & potential R&D
Theory development needed
  so-far only single SIS layer, extending it to (SI)N S needed
  interface properties (roughness/transition) not included
Several RF/DC measurements on samples show individual pieces of the puzzle are correct
  Pancake vortices & Hc,1 enhancement
  Higher Q0 above 5K or Tc of Nb
  Compensating individual flaws (Hysteresis, flux pinning)
  …
Show that it works! Proof-of-principle with an SRF cavity still pending (or with a QPR sample)
Two labs might not be enough → more resources / shoulders needed
Same argument as above: synergy with other fields (functional materials), use this leverage