## Slide 1: SRF theory for engineering an ideal surface for SRF cavities
Alex Gurevich
Old Dominion University, Norfolk VA
Supported by DOE under grant DE-SC0025560

## Slide 2
Reentrant shape
Single-cell: 59 MV/m (223 mT) 1.3 GHz at 2 K
53.3 MV/m in 650 MHz single-cell
Positive Q slope, high Q, highest breakdown fields
Negative Q slope, high Q, reduced breakdown fields
Dhakal, Ciovati et al.
PR STAB 16. 042001 (2013)
Grasselino et al, FNAL
Conundrum of SRF performance limits
How far can the breakdown fields and Q factors in best Nb cavities be increased?
SRF theoretical Q and H limits at T << Tc are unknown. Eliashberg instead of BCS is required to get reliable numbers for Nb and Nb3Sn
Is there a magic way to simultaneously push
both Q and H limits or they are mutually
exclusive?
Both Q and H limits can be be increased by
surface nanostructuring, even if we do not know
what the exact theoretical limits are.

## Slide 3: BCS surface resistance
Dirty:
normal skin
effect
Clean:
anomalous
skin effect


D.C. Mattis and J. Bardeen, Phys. Rev. 111, 412 (1958)
Is the optimal Q at GHz
frequencies and low T
limited by the idealized
BCS surface resistance?
Temperature-independent
residual surface resistance
Where is Ri coming from?
The factor
is minimum at = 20 nm
Moderately dirty surface
is best at low RF fields

## Slide 4: Broadening the DOS gap peaks reduces Rs
Low-frequency M-B surface resistance at 1-2 GHz, hf/kT ≈ 10-2
Idealized
BCS
Broadened gap
peak and subgap
states in the
Dynes model
Density of states with broadened gap peaks:
Rs can be reduced by:
electron-phonon scattering
proximity-coupled suboxides
dilute magnetic impurities
dirty layers at the surface
The log. term in Rs results from the singularity in the BCS DOS at ε = Δ
Broadening the gap peaks
can reduce Rs by 4-5 times

## Slide 5: Residual surface resistance from subgap states
Generalized M-B:
AG, SUST 30, 034004 (2017)
AG and Kubo, PRB 96, 184515 (2017)
Ri = 10 nohm at 1.5 GHz and nm at
Residual resistance is a part of BCS surface resistance which takes into account the broadening of gap peaks in
Ri increases with but Rs(T) at higher T is decreased by moderate DOS broadening
good
bad

## Slide 6
Current-induced broadening of DOS peaks causes a negative Q(H) slope
Subgap states caused by finite quasiparticle lifetimes.
Surface layer of reduced BCS pairing constant (surface nonstoichiometry)
Proximity coupled thin normal (suboxide) layer on the surface
Small density of magnetic impurities
S
N
magnetic
impurities
Gurevich, PRL 113, 087001 (2014)
Gurevich and Kubo, PRB 96, 184515 (2017)
Kubo and Gurevich, PRB 100, 064522 (2019)
Calculatioins of Rs in the dirty limit
based on the Usadel equations
Optimizing surface resistance by pairbreaking mechanisms
Current-induced DOS broadening
DOS oscillating under RF currents
Reducing Rs by engineering an optimum DOS by surface nanostructuring and impurity management
Surface resistance can be reduced by RF current, surface nanostructuruing and magnetic impurities

## Slide 7
Tuning Rs by magnetic impurities
is spin flip m.f.p
magnetic
impurities
An optimum density of magnetic impurities can significantly reduce Rs
corresponds to the spin flip m.f.p.
4μm

## Slide 8
Rs can be optimized by tuning the N-layer parameters.
Rs can be smaller than the ideal surface without N layer
Tuning proximity-coupled NbO metallic suboxide layer
Contact resistance RB can be changed
by orders of magnitude by heat treatments
AG and Kubo, PRB 96, 184515 (2017)
Nb
NbO
Nb2O5
d

## Slide 9: Broadening the DOS peaks by current produces negative Q slope
Maki, Prog. Theor. Phys. 29, 10; 333 (1963);
Fulde, Phys Rev. 137, A783 (1965)
Lin and Gurevich, PRB 85, 054513 (2012)
clean
dirty
The effect of current on the DOS:
Gap singularities are smeared out
The quasiparticle gap becomes
smaller than , both and
decrease with H
In the clean limit the gap vanishes at
H < Hs:
In the dirty limit the gap remains
finite at Hs:
Gurevich, PRL 113, 087001 (2014)

## Slide 10: What are the SRF field limits and how could they be raised?
The GL theory of dc superheating field Hs(T) is applicable near Tc but not at T << Tc.
Only Hs(0) = 0.84Hc at in the clean limit Catelani and Sethna, PRB 76, 224509 (2008)
and for arbitrary impurity concentration Lin and Gurevich, PRB 85, 054513 (2012) have been calculated.
Dynamic superheating field Hd(T,f) can be different from the static Hs(T) at GHz frequencies:
Sheikhzada and Gurevich, PRB 102, 104507 (2020)
Increase of Hs by surface nanostructuring: dirty layers, SIS or SNS multilayers for which Hs has only been calculated in the limit of
GL numerical calculations of Hs at realistic finite GL parameters of Nb and Nb3Sn:
Pathirana and Gurevich, Front. Electr. Mat. 3, 1246016 (2023)
  Dirty surface layers
  SIS structures: dirty Nb-I-clean Nb, Nb3Sn-I-Nb and others
A significant boost of Hs can be achieved by optimizing SIS parameters.

## Slide 11: DC superheating field
GL region, T ≈ Tc: (Matricon and Saint-James, 1967, Chapman 1995)
Bs decreases as the GL parameter κ = λ/ξ increases if the
material gets dirtier:
Raising simultaneously Q and H limits appears mutually exclusive
No theory of Hs(T) at low T and
Clean Nb
GL extrapolation to T << Tc underestimates Hs(0) = 0.84Hc at κ >> 1 in the clean limit (Catelani and Sethna, 2008)
and for arbitrary concentration of nonmagnetic and magnetic impurities (Lin and Gurevich, 2012)

## Slide 12: Vortices protect superconductivity at H > Hs
H0
At H < Hs screening currents are not strong enough to break the Meissner state at J(0) < Jd
z
At H > Hs vortices reduce the current density at
the surface allowing SC at higher fields
H < Hs
H > Hs
Counterflow of vortex currents against the Meissner current reduces J(0) at the surface below Jd allowing
SC to survive up to high fields Hc2 at which the vortex cores overlap
The SRF breakdown is limited by Hs but not Hc2
Vortices penetrate with supersonic velocities in
Embon et al Nat. Commun. 8, 85 (2017); Dobrovolskiy et al, Nat. Commun. 11, 3291 (2020)
Delay with penetration of vortices at H > Hs does not increase the SRF field limit but destroys SC

## Slide 13: Hs for nanostructured surfaces in the limit of
SIS London model
Gurevich, APL 88, 012511 (2006); AIP Adv. 5. 117112 (2015)
Kubo, Iwashita, Saeki, APL 104, 045006 (2014)
SIS, dirty limit, Usadel eqs
Kubo, SUST 34, 045006 (2021)
Ngampruetikorn and Sauls,
Phys. Rev. Res. 1, 012015 (2019)
Dirty surface layer
Inhomogeneous impurity
scattering rate at the surface
Enhancement of Hs by current counterflow induced in the overlaayer

## Slide 14: GL numerical calculations of Hs at finite
Partial suppression of
by
screening current at H < Hs
Growth of periodic perturbations
along the surface preceding
penetration of vortices at H > Hs
GL results for
GL numerical simulations for Nb:
Pathirana and Gurevich, Front. Electr. Mat. 3, 1246016 (2023)
Period along the surface
Decay length perpendicular to the surface
Christiansen, Solid Stat. Comm, 7, 727 (1969); Chapman
SIAM J. Appl. Math , 55, 1233 (1995); Transtrum et al, PRB
83, 094505 (2011), Liarte et al, SUST 30, 033002 (2017)

## Slide 15: Dirty layer at the surface
Slowly ramping magnetic field:
instability

## Slide 16: Detecting superheating field
x/ξ
Order Parameter (f)
y/ξ

## Slide 17: Dirty surface layer, results
Maximum in Hs(ld) results from current counterflow induced in the dirty surface layer with larger
by the cleaner bulk with smaller , similar to that in SIS multilayers. Reduced Hs at larger ld is due to
larger GL parameter of the dirty layer,

## Slide 18: SIS with the same materials
SIS Nb3Sn with the same
parameters of the overlayer
and the the bulk
SIS Nb3Sn with dirtier overlayer
Dip in Hs(d) at small d results from suppression
of vortex perturbations by I layer over
perpendicular to the surface
Dashed line: Hs(d) calculated in the London model
N-doped – I – clean Nb structures may outperform the best bare Nb cavities

## Slide 19: High-Tc overlayer in SIS
Nb3Sn - I - Nb
Thin Nb3Sn overlayer more
than doubles the dc
superheating field
London model works
surprisingly well
I interlayer is necessary to
prevent avalanche penetration
of vortices

## Slide 20: Blocking penetration of vortices by I layers
Kubo et al, APL, 104, 032603 (2014); SUST, 30, 023001 (2017); 34, 045006 (2021)
Posen, Transtrum, Catelani, Liepe, Sethna, Phys. Rev. Appl. 4, 044019 (2015)
Nb
dielectric layers
higher-TcSC: Nb3Sn, etc, etc
SIS multilayers (Gurevich, APL. 88, 012511 (2006))
Hm at the optimum thickness exceeds Hs of both Nb and the layer material. mT (dirty Nb layer),
I layer intercepts vortex loops and do not
let them propagate to the bulk
Strong decrease of vortex dissipation
NbN overlayer (Antoine et al, APL 102, 102603 (2013);
Roach, et al, IEEE Trans. Appl. Supercond. 23 (2013))
NbTiN/Al2O3/Nb thin film bilayers (Valente, SUST 29 (2016) )
Nb3Sn multilayers (Sundahl et al.Sci. Rep. 11, 7770 (2021) )
MgB2 coating of Nb (Tan et al, Sci. Rep. 5, 35879 (2016))
Experimental progress
Gurevich, AIP Adv. 5, 017112 (2015)
Maximum breakdown
field at an optimum
layer thickness
Higher Hm due to current counterflow at

## Slide 21: Challenges for the SRF theory
Switch from the MB model to the Eliashberg theory which describes realistic superconductors with strong e-p pairing (Nb, Nb3Sn, NbN etc)
Enigma of quasiparticle subgap states which define the ultimate Q limit at T<<Tc (SRF cavities and qubits). Many possible mechanisms (TLS, correlated impurities, strong e-p coupling, etc).
Field dependent Q(H) at high rf fields: Pandora box of nonequilibrium superconductivity and complex kinetics of superconductors under strong RF fields. e-p and e-e relaxation times and their strong dependencies on T and rf field
Extended Q(H) rise, the effect of nonequilibrium kinetics of quasiparticles or two-level states
Ultimate breakdown of superconductivity - the physics of dynamic superheating field at GHz frequencies at low T
Extreme dynamics of superfast tips of trapped vortices at the SRF depairing limit. Effect of trapped flux on the high-field Q slope

## Slide 22: Conclusions
What we know: the well-established BCS electrodynamics and trapped vortex losses at low rf fields. Effect of proximity coupled metallic precipitates or suboxide layers.
What we do not know or not fully understand:
Mechanisms of residual resistance, subgap states, TLS
Theoretical Q and H limits for key SRF players (Nb and Nb3Sn)
Theory of nonequilibrium superconductivity which describes Q(H) at high rf fields
Extreme dynamics of trapped vortices driven by rf fields in SRF cavities
The exact SRF performance limits are currently unknown. Yet the SRF performance
both at low and high RF fields can be improved by impurity management and surface nanostructuring, even if we do not know what the limits are.
Filling the knowledge gaps requires developing the Eliashberg + nonequilibrium theories of SRF limits in conjunction with advanced computational modeling.