## Slide 1: MKID Bolometer
Jack Bargemann
SLAC SSI 2026
jack.bargemann@pnnl.gov

## Slide 2: Radiation in a Qubit Substrate
gamma
gamma
hadron / alpha
muon
Ionizing radiation is a problem for qubits
Different types of radiation have different origins, produce different spectra, and require different shielding
muon

## Slide 3: A shallow underground lab
hadron
muon
muon

## Slide 4: PNNL Shallow Underground Laboratory and Low Background Cryogenic Facility (LBCF)
SUL houses clean rooms (class 10,000 and 1,000) , world-leading ultra-pure material growth and characterization capability
19 m overburden reduces muon flux by 6X, neutron and proton flux by >100X
Bluefors LD-400 dilution fridge with external gamma shield
Dilution Refrigerator

## Slide 5: LBCF Shield
Reduces gamma rate from surrounding earth and building material

## Slide 6: NIST Thermal Kinetic Inductance Detector
Energy-resolving qubit proxy

## Slide 7: Why use a thermal KID?
Reduced position-dependence!
A study of the position-dependent response of thermal kinetic inductance detectors through the use of cryogenic beam steering, Flogarty et. al.
With thanks to the SLAC DMQIS group for providing the steerable MEMS mirror

## Slide 8: NIST Thermal Kinetic Inductance Detector
Energy-resolving qubit proxy
Fast athermal signal
Slow thermal signal

## Slide 9: NIST Thermal Kinetic Inductance Detector
Energy-resolving qubit proxy
60 keV 241Am

## Slide 10: NIST Thermal Kinetic Inductance Detector
Energy-resolving qubit proxy
60 keV 241Am

## Slide 11: Do we really need to micromachine?

## Slide 12: Thermally Isolating the entire chip
copper housing
silicon substrate
solder wire thermal standoff
nylon screw

## Slide 13: Results – it works!

## Slide 14: Results – it works!
477 keV Compton shoulder
5.3 keV 210Po alphas

## Slide 15: Results – it works!

## Slide 16: Fixing 210Po alpha backgrounds
copper housing
silicon substrate
solder wire thermal standoff
nylon screw

## Slide 17: Fixing 210Po alpha backgrounds
copper housing
silicon substrate
solder wire aluminum spheres
nylon screw

## Slide 18: Low-background MKID bolometer
PRELIMINARY

## Slide 19: Future directions
Background measurement with 𝒪(several) gram-days of exposure
  (very) near future
Mount and operate low-volume-high-sensitivity MKIDs as bolometers
  With a well-optimized MKID, what energy and temperature sensitivity is achievable?
Improved chip mounting
  Nylon clamp screw was a stopgap
  Clips or pogo pins would allow reproducible clamping force
MKID arrays
  Arrays of MKID resonators should see a coherent thermal signal
    √n improvement in signal-to-noise when channels are summed
  Athermal signal can be used for position reconstruction, triggering

## Slide 20: Alphas and Radiopurity
Abatement of ionizing radiation for superconducting quantum devices
Alphas can only reach qubit substrates by line-of-sight
Significant sources of alphas:
  Beryllium-copper pins on SMA connectors
  Radioactivity in interposer circuit boards

## Slide 21: SMA Connectors
 |  |  | 232Th |  | 238U | 
Product No. | Material | Rep# | pg/g | +/-sd | pg/g | +/-sd
132147-29 | All dissolved (sans PTFE) | rep1 | 3100 | 200 | 24300 | 400
132147-29 | All dissolved (sans PTFE) | rep2 | 1400 | 200 | 1510 | 90
132147-29 | All dissolved (sans PTFE) | rep3 | 1070 | 90 | 1170 | 80
901-9201-2A | Nut Portion w/CuBe | rep1 | 14800 | 500 | 16200 | 8000
901-9201-2A | Nut Portion w/CuBe | rep2 | 14870 | 700 | 13100 | 2000
901-9201-2A | Nut Portion w/CuBe | rep3 | 15000 | 1500 | 15200 | 4000
901-9201-2A | CuBe Pin | rep1 | 230000 | 15000 | 2400000 | 18000
901-9201-2A | CuBe Pin | rep2 | 270000 | 13000 | 2500000 | 10000
901-9201-2A | CuBe Pin | rep3 | 250000 | 15000 | 2500000 | 40000
132101 | Brass Nut Portion | rep1 | 11 | 3 | 51 | 4
132101 | Brass Nut Portion | rep2 | 8 | 6 | 39 | 8
132101 | Brass Nut Portion | rep3 | <3 | - | 28 | 4
132101 | Brass Pin | rep1 | 28 | 10 | 5 | 5
132101 | Brass Pin | rep2 | 7 | 4 | 4 | 7
132101 | Brass Pin | rep3 | 9 | 2 | <1.2 | -
132248 | Steel Nut Portion | rep1 | 330 | 40 | 60 | 4
132248 | Steel Nut Portion | rep2 | 540 | 150 | 290 | 130
132248 | Steel Nut Portion | rep3 | 320 | 50 | 68 | 1
132248 | CuBe Pin | rep1 | 60 | 10 | 250 | 30
132248 | CuBe Pin | rep2 | 39 | 5 | 230 | 40
132248 | CuBe Pin | rep3 | 37 | 12 | 170 | 30
19S202-40ML5 | All (no CuBe) | rep1 | 4 | 6 | 3 | 5
19S202-40ML5 | All (no CuBe) | rep2 | <3 | - | <0.8 | -

## Slide 22: SMA Connectors
 |  |  | 232Th |  | 238U | 
Product No. | Material | Rep# | pg/g | +/-sd | pg/g | +/-sd
132147-29 | All dissolved (sans PTFE) | rep1 | 3100 | 200 | 24300 | 400
132147-29 | All dissolved (sans PTFE) | rep2 | 1400 | 200 | 1510 | 90
132147-29 | All dissolved (sans PTFE) | rep3 | 1070 | 90 | 1170 | 80
901-9201-2A | Nut Portion w/CuBe | rep1 | 14800 | 500 | 16200 | 8000
901-9201-2A | Nut Portion w/CuBe | rep2 | 14870 | 700 | 13100 | 2000
901-9201-2A | Nut Portion w/CuBe | rep3 | 15000 | 1500 | 15200 | 4000
901-9201-2A | CuBe Pin | rep1 | 230000 | 15000 | 2400000 | 18000
901-9201-2A | CuBe Pin | rep2 | 270000 | 13000 | 2500000 | 10000
901-9201-2A | CuBe Pin | rep3 | 250000 | 15000 | 2500000 | 40000
132101 | Brass Nut Portion | rep1 | 11 | 3 | 51 | 4
132101 | Brass Nut Portion | rep2 | 8 | 6 | 39 | 8
132101 | Brass Nut Portion | rep3 | <3 | - | 28 | 4
132101 | Brass Pin | rep1 | 28 | 10 | 5 | 5
132101 | Brass Pin | rep2 | 7 | 4 | 4 | 7
132101 | Brass Pin | rep3 | 9 | 2 | <1.2 | -
132248 | Steel Nut Portion | rep1 | 330 | 40 | 60 | 4
132248 | Steel Nut Portion | rep2 | 540 | 150 | 290 | 130
132248 | Steel Nut Portion | rep3 | 320 | 50 | 68 | 1
132248 | CuBe Pin | rep1 | 60 | 10 | 250 | 30
132248 | CuBe Pin | rep2 | 39 | 5 | 230 | 40
132248 | CuBe Pin | rep3 | 37 | 12 | 170 | 30
19S202-40ML5 | All (no CuBe) | rep1 | 4 | 6 | 3 | 5
19S202-40ML5 | All (no CuBe) | rep2 | <3 | - | <0.8 | -