## Slide 1
Tuning energy levels and energy flow in nanomaterials through the
external environment
Archana Raja
Feb 25, 2019
SLAC National Laboratory

## Slide 2
Sizes of things
Doug Natelson. Nanostrucutres and Nanotechnology.
Cambridge University Press (2015)

## Slide 3
Nanotechnology in history
Roman goblet with stained glass containing gold nanoparticles
British Museum
Micro- and nanostructured steel in Japanese katana swords
Yasoi et al. ESOMAT (2009)

## Slide 4
2 – 7 nm
Physical phenomena at the nanoscale limit
Structure & function
Interactions
with the local
environment
Nanoscale limit
Molecular picture
in different
solvents
<1 nm
{
Monolayer transistor
Quantum picture
L

## Slide 5
B. Radisavljevic et al., Nature Nano., 6, 147 (2011)
Nanoscale building blocks
0D quantum dots, fullerenes...
1D CNTs, nanowires...
2D graphene
Transition metal dichalcogenides
(TMDCs)

## Slide 6
Micromechanical exfoliation of 2D materials
2 Peel off a few layers
4 Monolayer on substrate
Substrate
Substrate
1 Bulk graphite, TMDC
3 Place layers on substrate
Adapted from: K. S Novoselov, Rev. Mod. Phys. (2011)

## Slide 7
Library of 2D materials
Graphene: semimetal
BN: insulator
MoS2, MoxW1-xS2, WS2: semiconductors
NbSe2: superconductors
CrI3: semiconducting ferromagnet
Adapted from: E. Gibney, Nature (2015)
Transition metal dichalcogenides
(TMDC)
Flexible atomic membranes, unique tunable optical and electronic properties!
Layered perovskites

## Slide 8
Bulk
4L
2L
1L
MoS2
A. Splendiani et al., Nano Lett., (2010)
Monolayers are direct-gap semiconductors
Chalcogen
p orbitals
Metal
d orbitals
Dramatic light matter coupling at the monolayer limit
Chalcogen
p orbitals
Light emission
Optical image
Few layers
Monolayer
G
K
M
kx
ky
Brillouin zone
K.F. Mak et al., Phys. Rev. Lett. (2010)

## Slide 9
Tuning nanomaterials using the local environment
Novel heterostructures for emergent physical phenomena
Atomically precise modulation of properties
Additional rotational degree of freedom: inter-layer twist
   recent reports of superconductivity in twisted bilayer graphene, bilayer graphene on hBN

## Slide 10
Part II
Part I
Egap
Today’s talk
Coulomb engineering of the bandgap and excitons in 2D semiconductors
Energy transfer from quantum dots to 2D materials

## Slide 11
Bandgap engineering
x
E
+ e/e repulsion
Valence band
Conduction band
+ e/h
attraction
Valence band
Conduction band
Valence band
Conduction band
Doping
Strain
Alloying

## Slide 12
Bandgap engineering in 2D regime
x
E
+ e/e repulsion
Valence band
Conduction band
+ e/h
attraction
Valence band
Conduction band
Modify the environment,
not the material
“Coulomb engineering”

## Slide 13
Excitons are a consequence of Coulomb interaction
Optical gap
Exciton
Energy
Bandgap
Free carriers
Binding energy
Effective mass
Dielectric screening
Hydrogen: 13.6 eV
Bulk TMDC, GaAs QWs ~10 meV
Room temperature 25 meV
Optical absorption
Schematic
Quantum number
Charge

## Slide 14
A. Chernikov et al. Phys. Rev. Lett. 113, 076802 (2014)
“Rydberg” spectroscopy of excitons:
non-invasive probe of the bandgap

## Slide 15
Energy
Optical absorption
~500 meV
Binding energy
t < 1 nm
Monolayer TMDC ~ 500 meV
Bulk TMDC, GaAs QWs ~10 meV
Room temperature 25 meV
A. Chernikov et al. Phys. Rev. Lett. (2014)
Z. Ye et al. Nature (2014)
M. M. Ugeda et al. Nat. Mat. (2014)
K. He et al. Phys. Rev. Lett. (2014)
…and many more
Optical gap
Exciton
Bandgap
Free carriers
L. V. Keldysh et al., JETP Lett. 29, 716 (1979)
K. Tanaka et al., Phys. Rev. B 71, 045312 (2005)
P. Cudazzo et al., Phys. Rev. B 84, 085406 (2011)
N. S. Rytova et al., Proc. MSU, Phys., Astron. 3, 30 (1967)
T. C. Berkelbach et al., Phys. Rev. B 88, 045318 (2013)
D. Qiu et al., Phys. Rev. Lett. 11, 216805 (2013)
Schematic
“Rydberg” spectroscopy of excitons:
non-invasive probe of the bandgap

## Slide 16
1s
Ground state
2s
Free electrons and holes at band-edge
Energy
D12
Binding energy
D12
Exciton
Ground state, 1s
Energy
Optical absorption
First excited state, 2s
Binding Energy ~ D12
Bandgap = E1s + Binding Energy
Schematic
“Rydberg” spectroscopy of excitons:
non-invasive probe of the bandgap

## Slide 17
Experiment: absorption-type measurements
Fused silica
White light
Spectrometer
Graphene
3L
1L
WS2
Measurement
spot
5 mm

## Slide 18
Monolayer WS2 excitons in different
dielectric environments

## Slide 19
Nanoscale sensitivity of the exciton states:
Experiment-theory comparison
Theory (QEH)
Experiment
Supp. WS2 (ES)
Supp. WS2 / graphite (ES)
Theory collaboration: Reichman group, Columbia University
Raja et al. Nature Commun., 8, 15251 (2017)
Also see: M. Rösner et al. Nano Lett. 16, 2322 (2016)
graphene
WS2

## Slide 20
Theory collaboration: Reichman group, Columbia University
EB = 290 meV
Bandgap
Exciton, n=1
EB = 120 meV
Raja et al. Nature Commun., 8, 15251 (2017)
Also see: M. Rösner et al. Nano Lett. 16, 2322 (2016)
graphene
WS2
Nanoscale sensitivity of the bandgap:
Experiment-theory comparison

## Slide 21
Dielectric in-plane heterostructure
ARPES collaboration with
Eli Rotenberg group at ALS,
LBNL
Raja et al. Nature Commun., 8, 15251 (2017)
Room temperature:
25 meV

## Slide 22
ARPES measures electron momentum and energy
 Dispersion of occupied electron states (valence bands)
Image source: arpes.stanford.edu
Angle resolved photoemission spectroscopy (ARPES)
ARPES at Lawrence Berkeley National Lab: 100 nm-10 µm spatial resolution

## Slide 23
Monolayer WS2 excitons in different
dielectric environments

## Slide 24
Band structure of monolayer WS2 in
different dielectric environments
Chalcogen
p orbitals
Metal
d orbitals
Chalcogen
p orbitals
~100 meV
Raja et al. In preparation

## Slide 25
Data offset by
core-level shifts
Band structure of monolayer WS2 in
different dielectric environments
Raja et al. In preparation

## Slide 26
Summary Part I
2D semiconductor: strong Coulomb interaction
Screening of exciton states in 1L WS2  Reduction in binding energy
Tune band gap over 100’s of meV by engineering dielectric environment
Nanoscale sensitivity
Future directions: dynamics of tuning dielectric environment, length scale and types of heterojunction

## Slide 27
Part II
Part I
Egap
Coulomb engineering of the bandgap and excitons in 2D semiconductors
Energy transfer from quantum dots to 2D materials
Today’s talk

## Slide 28
Core-shell semiconducting quantum dots  highly tunable absorption, high quantum yield
-- localized carriers inside core
+
2D materials  excellent transport of charge carriers
Non-Radiative Energy Transfer (NRET)
QD  2D

## Slide 29
_
NRET from QDs to graphene and MoS2
Distance
5.4 nm
Shell
CdZnS
Ligand
Core
CdSe
Layers of 2D material

## Slide 30
SiO2
Single QD photoluminescence
Grad

## Slide 31
MoS2
Graphene
PL quenching: QDs on graphene and MoS2
GNR
Grad
10x decrease in PL intensity

## Slide 32
_
PL
time
Total PL decay rate  slope
Time-resolved photoluminescence
via Time Correlated Single Photon Counting
Direct measurement of NRET rates

## Slide 33
Instrument response
On SiO2
On SiO2
QDs on SiO2 substrate

## Slide 34
On monolayer graphene
On SiO2
On SiO2
QDs on graphene
Rate ~ 1/Lifetime
Mono to bilayer graphene
On SiO2

## Slide 35
Increasing graphene
thickness
Increasing MoS2
thickness
QDs on graphene vs. MoS2

## Slide 36
MoS2
Graphene
QDs on graphene vs. MoS2
Raja et al. Nano Letters 2016.
Also see: Prins et al. Nano Letters 2014, Chen et al. ACS Nano 2010

## Slide 37
Screening 
 E field
Energy transfer rate 
0
1
|E|
Absorption vs. Screening
Graphene
MoS2

## Slide 38
NRET rates: experiment vs. theory
QD:point dipole, 2D:dielectric slab
Inputs: dielectric functions, QD size, acceptor thickness, decay rate in solution
No free parameters
Extendable for arbitrary 2D heterostructures
Chance, Prock and Silbey. Adv. Chem. Phys. 37, 1 (1978)
Gordon and Gartstein. J. Phys. Condens. Matter 25, 42 (2013)
Theory collaboration:
Andrés Montoya-Castillo,
David Reichman

## Slide 39
Efficient energy transfer QD  2D
 no. of layers, energy transfer rate:
   to graphene
   to MoS2
Dissipation vs. screening
Summary Part II

## Slide 40
Patterning electronic states and energy transport on an atomically thin canvas
Nanoscale lateral heterojunctions
Band gap
x
E

## Slide 41
Raja et al. Nature Commun., 8, 15251 (2017)
Proposed research at SLAC:
1. Electronic and structural dynamics of Coulomb Engineering
Tensile strain ~ 45 meV/%
Conley et al. Nano Lett. 13, 3626 (2013)

## Slide 42
Proposed research at SLAC:
1. Electronic and structural dynamics of Coulomb Engineering
Time-resolved optical spectroscopy
Ultrafast Electron Diffraction or LCLS
Lin et al. Nature Commun. 8(1) 1745 (2017)
Tunable
(e.g.: MoTe2)
Bandgap of WS2
WS2
Sub-bandgap
pulsed resonant
excitation

## Slide 43
Proposed research at SLAC:
2. Twisted 2D layers: Moiré excitons & non-equilibrium dynamics
condmat.physics.manchester.ac.uk/imagelibrary

## Slide 44
Proposed research at SLAC:
2. Twisted 2D layers: Moiré excitons & non-equilibrium dynamics
Yu et al. Sci. Adv. 1701696 (2017)
MoS2 / WSe2
Ultrafast optical
spectroscopy
θ
Longer pulse sets
equilibrium structure
Short pulse resets to
non-equilibrium structure
Ultrafast structural
dynamics

## Slide 45
Acknowledgments
James Hone
Ghidewon Arefe
Jaeeun Yu
David Reichman
Andrey Chaves
Tim Berkelbach
Tony F. Heinz
Louis E. Brus
A. Montoya-Castillo
Alexey Chernikov
A. Paul Alivisatos
Eli Rotenberg
Aaron Bostwick
Chris Jozwiak
Roland Koch
Lutz Waldecker

## Slide 46
Part I: Coulomb engineering of the bandgap and excitons in 2D semiconductors
Raja et al. Nature Communications, 8, 15251 (2017)
Part II: Transport of excitons across 0D/2D interfaces – dielectric screening and absorption
Raja et al. Nano Letters, 16(4), 2328 (2016)
archana.raja@berkeley.edu
Tuning nanomaterials using the local environment

## Slide 47
Appendix

## Slide 48
Thickness (nm)
Energy transfer rate
Engineering energy transfer: predictions
= 1 Graphene-like behavior
> 1 MoS2-like

## Slide 49
Energy transfer vs. Charge transfer
Peng et al. Nano Lett. 2011

## Slide 50
Effect of the QD shell on NRET

## Slide 51
Lateral confinement in the 2D plane
2
3
4
2
3
4
Energy (eV)
Optical Absorption
Energy (eV)
> 20 nm
< 10 nm
20 nm
Liquid phase exfoliation: similar to bulk
Colloidal synthesis:
1 eV blue-shift
Solution processed MoS2
TEM image of colloidally synthesized MoS2 quantum dots

## Slide 52
Angle resolved photoemission spectroscopy (ARPES)
R. Schlaf, http://rsl.eng.usf.edu/

## Slide 53
W. Liptay, ”Electrochromism and Solvatochromism”, Angew. Chem. (1969)
2D limit: solid state version of molecules

## Slide 54
Theory predicts type II heterojunction
Rösner et al. Nano letters (2016)

## Slide 55
Theoretical “road map”
20
10
8
6
4
2
1
1
20
10
8
6
4
2
eTop
eBottom
500
400
300
200
100
< 25
Eb (meV)
eBottom
eTop
WS2
graphite
hBN
SiO2
TMDCs

## Slide 56
Fabrication: WS2 & graphene

## Slide 57
Atomic-force microscopy

## Slide 58
Graphene-encapsulated WS2

## Slide 59
WSe2 structures

## Slide 60
Emerging applications
lasers
Electronics
Catalysis
transistor
Deng et al. Nature Nano. 2016
Jariwala et al. ACS Nano 2014
Photonics and photovoltaics
Mak and Shan. Nature Photonics 2016