## Slide 1: Nanosecond imaging at LCLS with UXI detectors
Philip Hart, Ulitima 2022 2023
So far, this year, and the future
Few Pico?

## Slide 2: Outline
Intro to UXI detectors
Past work with Icarus at LCLS
Ongoing science
Problems
Harder problems
Bright future

## Slide 3: Local perspective (250ms frame rate)
350ps *1012
Magnitude/decade

## Slide 4: ... impractical setup

## Slide 5: UXI collaboration and Icarus
Ultrafast X-ray Imager family of detectors from Sandia
  …, Icarus, Daedalus, Tantalus, …
  Icarus takes 4 frames in 8 ns (or longer)
  25 um Si sensor, 25 um pixel pitch, 2.5x1.3 cm, 1 (10?) Hz, EMP hard, can see single photons at 6 keV, full well ~250 photons
    GaAs sensors in packaging
  Sensor/asic built at MESA (very not commercial process, high demand at Z machine, NIF, Omega)
  Readout we use comes from LLNL -> integrated in DAQ
We have collaborated since 2017
  We get sensors for expts, some input on new features
  They get calibration data with LCLS beam + diagnostics
  Several in house, in house + user experiments at LCLS
Detectors built with non-commercial process; imperfect
  Spinoff company AHS developing commercial design
    See talk tomorrow by Liam Claus
  SBIR with Sydor to get features we want underway

## Slide 6: Why do we want this?
The accelerator gives us four pulses down to 350ps separation
Burst mode imagers give us access to ns-scale science
  E.g. shock propagation in materials, ICF implosion dynamics
  XPCS (would work if we could run at 120 Hz) (will work when…)
  Next UXI version designed to reach 500 ps; 300 ps possible
    proposed SparkPixDelta would reach this (accumulation mode)
Multiple frames in a time scan on one pumped sample
  Esp. valuable for low-rate optical laser expts that blow up targets
Gate away unwanted time-dependent backgrounds
100x time magnification with HSLOS (pulsed dilation tube, https://aip.scitation.org/doi/full/10.1063/1.5039648) to reach <30 ps science with split/delay etc.

## Slide 7: Current “1-2” time structure for 4 pulses at LCLS
(1+2)ns period just fits this pulse pattern. We spent a few minutes fine adjusting frame timing during last experiment
8ns
Debye
Scherrer
Icarus sensor
Readout board in fancy housing

## Slide 8: Highlights from “First x-ray test of the Icarus nanosecond-gated camera at LCLS” (doi: 10.1117/12.2520974), Hart et al.
Pump energy
Pumped frames
Cold Cu
Hot Cu

## Slide 9: ICF void collapse: MEClv08 (above, XPCI, Nov 2020) MECx493 (below, direct illumination, 10ns flat top drive)
From Hodge et al., 2022
40x magnification at detector (25 um pixels) with Be CRLs

## Slide 10: See Optics Express, “Multi-frame, ultrafast, x-ray microscope for imaging shockwave dynamics”, 2022
We combined the four-pulse bunch train at LCLS with the MEC optical laser as a drive to study void collapse for inertial confinement fusion. Hodge et al. extract the mass density of the target as the shock passes through and compare the propagation to a simulation of the development of hydrodynamic instabilities. Expected “jetting” is apparent. Shock wave is observed to split around the void.

## Slide 11: Next expt: imaging laser powder bed fusion (3d metal printing) from 2-200ns – Leora Dresselhaus-Marais et al.

## Slide 12: Later this year
Plan to extend study of shocked Si with 9 keV X-rays to shocked Ge with 17 keV X-rays
  Requires GaAs sensor to achieve reasonable QE
    UXI folks working on packaging challenges
Deploy Icarus sensor in vacuum (first for LCLS)
Demonstrate stability, ease of 4-pulse configuration
  Requirement for user experiments in 2024
Si shock dislocations

## Slide 13: Problems just requiring work
Last expt.
  Had some DAQ/controls instability
  Setup involves a lot of discrete components (PS, delay gen.)
  Trouble getting the X-ray pulses to lase consistently
    Issues with laser table
    Lack of fast monitoring feedback for tuning
Be (de)focusing X-ray lenses leave artifacts
White field

## Slide 14: Laser table, beam monitoring improvements underway
Upgrade table components, motorize, expand
Add insertable, faster diode, better cabling for feedback
  Allow tuning of multipulses independent of work in hutch
Fast diode trace from digitizer
with templated fit

## Slide 15: Tantalus is the first UXI ROIC designed in a commercial foundry
TowerJazz CA13SAV 130 nm process node
Designed as a test chip
  5 different pixel variants
  7 different oscillators
  120+ Hz readout
  500 ps integration time
Functional electrical testing completed
Next step is functional testing in radiation environment
Hybridization to demonstrate optical performance at speed
Iterate to implement a full array of optimal pixel variant
Requirement | Goal
Array size | 1024 x 512
Pixel size | 25 um
Number of frames | 4
Min Tint | 500 ps
Min inter-frame time | 500 ps
Timing skew | < 10%
Frame-Frame gain error | < 10%
Rep rate | 150 FPS
Full well | 500 ke-
Noise floor | < 250 e-
Dynamic range | > 60 dB
Slide from Liam Claus’s Ulitima talk
500*2 ps -> could run 700 ps bursts in
700 + 1400 + 700 ps pattern: 4 pulses in 2.8 ns

## Slide 16: Challenges
Science motivations for
  High QE, fast sensors
    High Z materials in active development in UXI collaboration, many other places
    See also e.g. talk tomorrow from Dominic Greiffenberg
  Large area (8x8 cm**2) detectors with high (>85%) fill factor
    Requires tiling (not currently abuttable) -> TSVs?
    Easily available large #s of detectors
  Stable, well-characterized cameras for precision science
    Current UXI detectors suffer from ringing due to inductance
    Related (?) cross-talk at high flux
    Can’t be cooled
  Smaller, larger pixel applications
  More frames (16?)

## Slide 17: Ce liquid-liquid transition and ejecta at 25keV
Motivation
-liquid polymorphism is of great importance in understanding the nature and physics of liquids
-f-electron nature of a material – localization vs. deloc. of f-electron dictates material behavior
-liquid-liquid transition established as extension of solid Ɣ-α phase transition (e.g., Cadien et al., 2013)
-anomalous melt boundary
Goals
shock melt polycrystalline Ce and follow subsequent liquid-liquid transition on release using transmission-geometry XRD in co-linear shock propagation direction – X-ray probe
Image shock wave propagation in Ce in a transverse shock propagation direction – X-ray probe geometry to follow solid phase transformation to melt sequence; image ejecta formation; use XRD probe to spatially resolve phases in the jets
Why 25 keV is required: higher quality liquid diffraction to discern between coordination changes in the melt; imaging of higher Z, very reactive material !!
  More than 4-fold extension of Q-range from 3.26-1 at 5.6 keV to 14.53 -1 at 25 keV – the only way to get reliable pair distribution functions
  Can’t just make Ce foils thinner to achieve higher pressures or increase X-ray transmission – no passivation layer
Cadien et al., 2013
Courtesy PI C. Bolme, 2017
Slide from A. Gleason

## Slide 18: Sensor issues – will physics allow us to get to 350ps and 25keV? (75 keV in 3rd harmonic?)
Transversal time of carriers is non-trivial at 1ns, 25um
  25um, 50V -> 2*104 V/cm -> 5*106 cm/s for holes in Si
  Flat distribution in depth -> 0.5ns spread in arrival at ASIC
    Limits minimum gate width
    Can do better at higher bias, cold: ~30-40%; or collect e-
      Can also do better with new materials, e.g. GaAs
        20um GaAs sensors expected next summer [2020]
QE for FEL hard X-rays is poor in Si at 25um
  ~0.5 at 6keV
New materials
  Don’t care about leakage at least at sub-ns collection times
  Important in many applications – collaboration is vital
This summer?

## Slide 19: PS regime
Pulsed dilation tube (SLOS-TRXI, HSLOS) technology allows ~100x time magnification with good (~6 um) spatial resolution
  Tech in use for ~ a decade at OMEGA, NIF
  With Icarus, can image at 25 ps
  If Tantalus can frame at 500 ps -> 5 ps regime?
    Presumably challenging to fight timing jitter
      Might need to sort through the data afterwards
Not a trivial undertaking to integrate

## Slide 20: MEC-U (2028)
Everything at MEC but scarier: petawatt laser -> more EMP -> harder detectors farther away -> more pixels

## Slide 21: The future is very exciting, but lots of work
Just some of the people/groups I’m working with who are doing the work:
UXI collaborators at Sandia, LLNL, Rochester
  A. Carpenter, Q. Looker, M. Wood, on and on
Advanced hCMOS Systems
  M. Sanchez, L.Claus, M. Dayton
At LCLS
  MEC (E. Galtier, B. Nagler, HJ Lee, D. Khagani, G. Dyer)
  Multipulses (FJ Decker, N. Burdet, S. Vetter)
  Fast feedback (S. Möller, A. Halavanau)
  DAQ (D. Damiani, M. Browne)
  XCS (D. Zhu, M. Seaberg)
  Users (A. Gleason, R. Sandberg, L. Dresselhaus-Marais, …)