## Slide 1
Surface Engineering Research for High Q and High Gradient CW Accelerators
Daniel Bafia
May 16th, 2023
LCWS’23
FERMILAB-SLIDES-23-067-TD

## Slide 2: Overview
Key Material Science Findings: Oxygen Enables High Q and G in LTB Cavities
Role of Diffused Oxygen in Mitigating HFQS
Role of Diffused Oxygen in Tuning Cavity Quench Field
Applying Findings to Cavities of Other Frequencies
What Other impurities?
Conclusion

## Slide 3: Quest for High Q0 and Gradient with Impurities
f0 = 1.3 GHz
T = 2 K
Nb SRF Cavities Post Various Surface Treatments
HFQS

## Slide 4: Quest for High Q0 and Gradient with Impurities
f0 = 1.3 GHz
T = 2 K
Nb SRF Cavities Post Various Surface Treatments
N impurities
High Q0: N-doping
High Gradient: N-Infusion
HFQS

## Slide 5: Quest for High Q0 and Gradient with Impurities
What is the precise role of O impurities in bulk Nb cavity performance and how can we tune performance?
f0 = 1.3 GHz
T = 2 K
Nb SRF Cavities Post Various Surface Treatments
HFQS
N impurities
High Q0: N-doping
High Gradient: N-Infusion
Oxygen impurities:
High Gradient: Low Temp. Bake
High Q0: O-doping
D. Bafia | LCWS 2023

## Slide 6: Key Material Science Findings: Diffused O Enables High G in LTB Cavities
A. Romanenko, TTC’2020, CERN
A. Romanenko et al, SRF’2019, THP014
Fick’s law diffusion
EP
LTB
TOF-SIMS Data on Cavity Cutouts
RF Data on Variously Processed Cavities to be Cut
What happens to RF performance if we gradually diffuse more oxygen?

## Slide 7: Utilizing Diffused O to Eliminate HFQS & Improve Gradient
As O diffuses deeper:
HFQS onset increases
Quench field improves
TE1RI003 Post Sequential 120C Baking
Calculated O Depth Profile
D. Bafia et al, Proceedings of SRF’2021, THPTEV016
2K
1.3 GHz
Subjected TE1RI003 to sequential rounds of 120 C vacuum baking
HFQS onset

## Slide 8: Solidifying the Role of O in the Mitigation of HFQS in 1.3 GHz
Onset of HFQS vs O Diffusion Depth
Before baking
After LTB
Supports Romanenko model of hydrides and shows that diffused oxygen mitigates HFQS
D. Bafia et al, Proceedings of SRF’2021, THPTEV016
33x decrease

## Slide 9: Diffusion Depth vs Quench Field for 1.3 GHz Cavities
HFQS regime: quench due to thermal origins
Quench peak
  When O diffuses 46 nm
   Achieved via 120 C x 12 hrs
HFQS Regime
Mid-T Bake data comes from S. Posen et al., PRA 13, 014024 (2020)
Quench Peak

## Slide 10: Applying 120 C x 12 hrs LTB to Other Frequencies: 650 MHz
What do we expect after 120 C x 12 hr in situ LTB?
No HFQS up to 161 mT
2) Quench @ 187 mT

## Slide 11: Applying 120 C x 12 hrs LTB to Other Frequencies: 650 MHz
What do we expect after 120 C x 12 hr in situ LTB?
No HFQS up to 161 mT
2) Quench @ 187 mT
  We observe 158 mT

?

## Slide 12: Applying 120 C x 12 hrs LTB to Other Frequencies: 650 MHz
What do we expect after 120 C x 12 hr in situ LTB?
No HFQS up to 161 mT
2) Quench @ 187 mT
  We observe 158 mT
  And again at 164 mT

?
Near record quench in 650 MHz, 164 mT!
Notes: Current record held by Sha et al. from CEPC with 168 mT at surface (achieved 40 MV/m but with Bp/Eacc = 4.2 mT/MV/m due to larger beam pipe diameter)

## Slide 13: Applying 120 C x 12 hrs LTB to Other Frequencies: 2.6 GHz
What do we expect after 120 C x 12 hr in situ LTB?
No HFQS up to 161 mT
Quench @ 187 mT

## Slide 14: Applying 120 C x 12 hrs LTB to Other Frequencies: 2.6 GHz
What do we expect after 120 C x 12 hr in situ LTB?
No HFQS up to 161 mT
Quench @ 187 mT
  We observe 160 mT

?
High quench field achieved in 2.6 GHz, 161 mT!
Preliminary: For same O profile, all cavities exhibit same HFQS and similar quench behavior regardless of frequency

## Slide 15: Further Surface Engineering Studies on Cavities
H. Hu
K. Howard
H. Hu et al., Proc. Of IPAC’23, WEPA190
K. Howard et al., Proc. of IPAC’23, WEPA189
Coupling simulation, material science, and RF testing to identify optimal oxygen profile for high Q0 and G in variously treated cavities
Comparative in-depth study of high and low RRR cavities to identify potential role of intrinsic impurities
Study on Role of Various Impurities in Cavities
Further Improving Cavity Performance with O
Looking for an enthusiastic postdoc to join our group!

## Slide 16: Conclusion
Oxygen diffused from the native niobium oxide via vacuum baking responsible for performance variation in cavities
1.3 GHz Cavity studies
HFQS onset scales linearly with the depth to which oxygen diffuses
Nonmonotonic relationship between quench field and O diffusion depth
Applied findings from 1.3 GHz cavities to other design frequencies and achieved near record gradients in 650 MHz and 2.6 GHz cavities
Studies to further improve performance underway:
  Profile tailoring, role of intrinsic impurities, …

## Slide 17: Thank Your for Your Attention!