## Slide 1: Photocathode Trends & High Gradient Hopes
John Smedley

## Slide 2: Overview
Cathode Overview
Semiconductor Cathodes
Principle of operation, Roughness, in situ x-ray analysis
Major Trends in Cathode Research
Epitaxy, Heterostructuring, Optical etalons, Sealed photocathode
What would a high gradient cathode look like?
The electron source determines the initial volume of phase space – and it is hard to make it better

## Slide 3: The means to generate electron beams
Solid
Vacuum
T = 0
Solid
Vacuum
T >0
Thanks to Jared Maxson, Cornell
Notes: So how do you get an electron beam? Start with a electrons in a box as a simple model of a metal.
Turn the temperature up, you get a tail of electrons extending above the fermi level.

## Slide 4: The means to generate electron beams
Solid
Vacuum
T >> 0
Thermionic Emission
Solid
Vacuum
T >0
Field emission

## Slide 5: The means to generate electron beams
Solid
Vacuum
T >0
Photon energy
Photoemission
Vacuum
T >0
Scattering loss
time

## Slide 6: Semiconductor Photocathodes
The primary path to high average current in photoinjectors
The good points:
  QE can be >10%
  Many use visible light
  Polarized cathodes possible
Common types:
Cs2Te – QE ~7% @ 262 nm, Lifetime ~1yr
K2CsSb – QE >4% @ 532 nm, Lifetime ~weeks
Cs:GaAs – QE ~0.5% @ 800 nm (polarized), >6% @ 527 nm
  W.E. Spicer & A. Herrera-Gomez, Modern Theory and Applications of Photocathodes, SLAC-PUB-6306 (1993)
However:
  Require UHV (<0.1 nTorr)
  Limited Lifetime
  Response time
  Complicated

## Slide 8: Maximum Achievable Brightness
Brightness limited by photocathode MTE
Child-Langmuir law
Ez (5-100+ MV/m)
Photocathode
Laser pulse
Electron Bunch
Increase
I. Bazarov et al., Phys. Rev. Lett. 102, 104801 (2009)

## Slide 9: MTE limiting factors -Surface non-uniformities
Physical Roughness
Chemical Roughness
S. Karkare and I. Bazarov, Phys. Rev Applied, 4, 024015 (2015)
J. Feng, S. Karkare et al, J. Appl. Phys. 121, 044904 (2017)
G. Gevorkyan et al. Phys. Rev. ST- Accel and Beams, 21, 093401(2018)
Combined Physical and Chemical Roughness
Need single crystal ordered surfaces to get sub-10 meV scale MTE

## Slide 10: K2CsSb: A Good Candidate
Unproductive absorption
In “magic window”
Onset of e-e scattering
T. Vecchione et al., Appl. Phys. Lett. 99, 034103 (2011)
Good Lifetime 1e-9 mBar
Low transverse Momentum (543 nm)
0.36 µm/mm
Caveats: Reflection mode Green light QE

## Slide 11: Traditional Sequential Deposition of K2CsSb High QE and Rough Surface
  S. Schubert et al., APL Materials 1, 032119 (2013)
  T. Vecchione, et al, Proc. of IPAC12, 655 (2012)
  25 nm roughness, 100 nm spatial period
  Emittance vs field measured with Momentatron, 532 nm light

## Slide 12: In operando analysis during growth (setup at NSLS/X21 & CHESS G3 & NSLS-II/ISR)
XRF
In-situ UHV growth system (10-10 ~ 10-11Torr)
installed at G3, CHESS
1/2/3: Evaporators
❶
❸
Synchrotron Radiation
+ : high brilliance, …
- : limited beamtime
9
3
9
0
8
7
10
Phi
15 20 25
2 theta
X-ray diffraction
Reflective spot
X-ray reflectivity
25 30 35 40 45 50 55
2θ
Wide angle X-ray diffraction
X-ray fluorescence
Growth and characterization system
15

## Slide 13: Experimental set up: K2CsSb cathode growth
16
Horizontal evaporation of three sources:
140
25
T(C)
t
Sb
K
Cs
Recipe:
100
X-rays
Sb
Cs K
FTM
P=1x10-10 mbar
t
QE during growth (532 nm laser)
Cs
QE(%)
K

## Slide 14: Reaction Dynamics
Antimony evaporated on Si, 0.2 Å/s; crystallize at 4nm
K deposition dissolves Sb layer - This is where roughening occurs!
QE increase corresponds with KxSb crystallization Cs increases lattice constant and reduces defects
M. Ruiz-Osés et al., APL Mat. 2, 121101 (2014)

## Slide 15
Ternary Co-evaporation Simultaneously evaporate from Sb evaporator and K,Cs effusion cells
Cs Cell
K capsule
J tube
Growth rate are controlled by J tube temperature, valve and shutter
Stoichiometry controlled by real time XRF

## Slide 16
(222)
(420)
(422)
(440)
Thickness
Real time
XRD
Real time
Fluorescence
QE
~10nm

## Slide 17
Stoichiometry & Structural Analysis
Camera 2
Highly textured
K2CsSb phase!
mm size lateral grains
Camera 1
Grain size 20.2nm
(220)
(111)
(222)
Grain size 27.7nm
(400)
(200)
 | K | Sb | Cs
L004 Si | 2.50 | 1.00 | 1.16
L005 Si | 2.37 | 1.00 | 0.91
L006 Si | 2.21 | 1.00 | 0.95
L011 Si | 2.07 | 1.00 | 0.94
L012 MgO | 1.98 | 1.00 | 0.88
Good K/Cs/Sb ratio!
This works for the entire Alkali antimonide family – we’ve created pseudo single crystals with a wide range of stoichiometries

## Slide 18
 | QE@532nm(%) | Roughness(A) | Thickness (A) | Grain size (A)
L004 Si | 4.9 | 3.5 | 234 | 155
L005 Si | 5.8 | 11.5 | 815.3 | 277
L006 Si | 5.4 | 13.8 | 757.5 | 202
Surface Roughness & QE
Simultaneous evaporation of all constituents results in no crystal phase transformation
Smooth, reproducible and ultra-high QE. Highly Crystalline!

## Slide 19: Co-deposition leads to efficient and ultra-smooth cathodes
Co-deposited K2CsSb yield spectrum
Sequential deposition
Co-deposition
20 MV/m
- significant emittance degradation for sequential method
- no practical degradation with co-deposition
LN2 threshold emission
  significant degradation, even with co-deposition
  we need films smoother than 0.6 nm!!
20 MV/m
5 MV/m
100 MV/m
J. Feng et al., J. Appl. Phys., 121(4) 044904, 2017

## Slide 20: Experimental set-up: Cs-Te cathode growth
Cam1:
XRD, XRR
Cam2:
XRD
Cam3:
XRF
Substrate
X-ray: 13 keV
LDLS Lamp source
Cs cell
Te
source
Te
Lα
Te
Lβ
Cs
Lβ
Cs
Lα

## Slide 21: Sequential vs Co-dep CsTe -- XRF
Sample | Te | Cs (+/-0.05)
R008 Sequential | 1.00 | 1.75
R009 Co-dep | 1.00 | 1.98
At same substrate temperature; co-dep method incorporates more Cs.
Te
Lα
Te
Lβ
Cs
Lβ
Cs
Lα
Si substrate
Cs deposition
@ 120 °C
Te deposition
@ 120 °C
Cs Te Co-deposition
@ 120 °C
Leave Cs on for a while
@ 120 °C

## Slide 22: Realtime analysis : Sequential growth
In less than 10 nm of Cs deposition, at least 2 intermediate phases appeared and disappeared, then a stable product of CsTe forms.
Te rate : 0.05 ~ 0.07 A/s
Cs rate : 0.2 ~ 0.6 A /s
~2nm
< 10nm
23.5nm
~150 nm

## Slide 23: Realtime analysis : Co-deposition
~25nm
~230nm
Starts to crystalize ~ 25 nm of total thickness.
Same phase throughout the growth.
CsTe rate : 0.2 ~ 0.6 A /s

## Slide 24: CsTe cathode Quantum efficiency
Co-dep can result in much higher QE than sequential
over cesiation might lead to Cs build-up on the cathode surface and lower the QE
QE can be recovered by removing the access Cs
QE
Wavelength (nm)
M. Gaowei, J. Sinsheimer, D. Strom, J. Xie, J. Cen, J. Walsh, E. Muller, and J. Smedley
Phys. Rev. Accel. Beams 22, 073401 – Published 23 July 2019

## Slide 25: CsTe cathode surface roughness: XRR analysis
 | Thickness (Å) | Roughness (Å)
FINAL Cs2Te/Cs2Te | 968.3 ± 2.9 (total Cs2Te) | 19.1 ± 0.2
Cs2Te/Cs2Te | 1026.1 ± 1.6 (total Cs2Te) | 19.10 ± 0.07
Cs2Te | 245.5 ± 1.7 | 9.55 ± 0.14
Si Substrate | - | 3.75 ± 0.02
R008 Sequential - CsTe on Si
Te/Si
Cs2Te/Si
Too rough to fit roughness
R009 Co-dep - CsTe on Si
Si
Cs2Te/Si
Cs2Te/Cs2Te/Si
Final Cs2Te/Si
Stopped growth temporarily
After growth
After Loadlock

## Slide 26: Trends and observations
Modern photocathode development is focused in two areas:
High average current (e- cooling, CW FEL – FLASH, EuXFEL, LCLS-II)
Ultra high brightness (UED/UEM)
These are driving development of semiconductor cathodes
Spatial uniformity (better than 0.6nm RMS), Single crystal
Ultra thin/optical etalon
Sealed photocathode systems for commercial delivery
Graphene or HBN covered cathodes
J. Biswas, et al., APL Materials 10, 111115 (2022)
H. Yamaguchi, et al., npj 2D Materials and Applications, 12, (2017)
A. Alexander, et al., AIP Advances 11, 065325 (2021)
J. Smedley, et al., Alkali Antimonide Photocathodes for Everyone, PAC 2013, 1178
Galdi et al., Appl. Phys. Lett. 118, 244101 (2021)
M. Gaowei, et al., Phys. Rev. Accel. Beams 22, 073401 (2019)

## Slide 27: Concerns at Ultrahigh gradient
Practical/Engineering – How to bring the cathode into the cavity?
Joints allow separation of problems, often at the cost of field emission
Cathode Field Emission – How to limit?
Higher work function or band gap, spatially smooth and uniform
Compromise on UV light?
Cesium migration? Will cathode poison the gun?
Requires R&D, but surface layers may help
Maintaining MTE at high gradient
Requires ultra smooth, possibly single crystal
1 nm RMS @ 250 MV/m, 1 nC bunch at CL limit: .06 um emittance from field

## Slide 28: What would optimal high field cathode look like?
Ultrasmooth – may need specialized growing surface with RA below 0.5 nm
Semi-epitaxial – limit boundary scattering and nonuniformity.
Evidence of epitaxy of Alkali antimonides on graphene is promising
Need defect control to allow doping of semiconductors to shift fermi level
“Smooth” layer
potentially graphene
Photoemissive layer
Visible sensitive
Alkali antimonide
Conducting layer
for charge resupply
at cryo
High Band Layer
Ideally p-doped
Alkali telluride
Laser
e-