## Slide 1: An ICP-MS based monitoring methodology to inform dust radioactive backgrounds on detector materials
Maria Laura di Vacri
S. Scorza, A. French, N.D Rocco,
T.D. Schlieder, I.J. Arnquist, E.W Hoppe, J. Hall

## Slide 2
Background mitigation in ultrasensitive detectors
Underground facilities and detector shielding
Ultrapure material sourcing
Uranium-238
Thorium-232
Images from
By Tosaka - Own work, CC BY 3.0, https://commons.wikimedia.org/w/index.php?curid=5531106
SuperCDMS detector

## Slide 3
The challenge
Bq/kg from Th, U, K
https://pubs.usgs.gov/of/2005/1413/maps.htm
1 ppt Th = 4.1 mBq 232Th/kg
1 ppt U =12.4 mBq 238U/kg
1 ppb natK = 30.5 mBq 40K/kg
Material radiopurity requirements ≈ mBq/kg
Sourcing
Selection
  Ultrasensitive analytical methods
Contamination
  Handling
  Exposure: DUST
    Even more problematic in underground facilities
11/08/2023

## Slide 4
Dust background monitoring
X-ray fluorescence (XRF) analysis for Th and U proxy elements (e.g., Ca and Fe)
Optical and fluorescence microscopy analysis
Backgrounds predicted based on dust fallout models and assumed composition
Boger, Jea, et al. "The Sudbury neutrino observatory." Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 449.1-2 (2000): 172-207
Akerib, D. S., et al. "The LUX-ZEPLIN (LZ) radioactivity and cleanliness control programs." The European Physical Journal C 80 (2020): 1-52.

## Slide 5
Direct, ICP-MS based method
2. Dissolution and analysis on a triple quadrupole inductively coupled plasma mass spectrometer (ICP-MS, Agilent Technologies)
Sensitivity on 232Th and 238U (30-day collection, class ≈1000 cleanroom)
10-3 fg·day-1·cm-2, or 10-8 mBq·day-1·cm-2
1. Dust sample collection on low-background vials
3. Determination of stable elements and long-lived radionuclides
4. Determination of fallout rates contaminant/surface/time

## Slide 6
The SNOLAB facility
A ≈ 5000 m2 class-2000 cleanroom
2 km underground, in the working Creighton nickel mine (operated by Vale Ltd.)
Hosting neutrino and dark matter experiments
Dust control is crucial

## Slide 7
Evaluation of SNOLAB mitigation procedures
Relevant to low-background detectors
Tracers for dust from mine and local rock*
2-4 replicates per location
Visible particulate found in some of the replicates
L9
L2
*I. Lawson, Analysis of rock samples from the new laboratory, STR-2007-003 SNOLAB technical report (2007)

## Slide 8
Results
Radionuclides of concern [mBq•day-1•cm-2]
Shaded areas refer to locations that are not maintained at cleanroom levels
A reference value for Pb specific activity from 210Pb (200 Bq·kg-1*) was used to infer 210Pb fallout rate
*Alessandrello, A., et al. Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms 142.1-2 (1998): 163-172.

## Slide 9
Results
Tracers for rock and mine dust [pg•day-1•cm-2]
Shaded areas refer to locations that are not maintained at cleanroom levels
Mine dust tracer

## Slide 10
Results
Monitoring location L6 during construction of a Pb shield
S1, S2  Two locations around the Pb shield assembly area
L6  Data collected while no Pb was being handled
Error bar hidden by marker in S2
HPGe measured 210Pb in the material: (4.2 ± 1.0) Bq·kg-1*
* p-type Canberra Well Detector, 46 keV line, ≈50g sample
210Pb fallout rate from the handled material [mBq·day-1·cm-2]:
  S1: (2.0 ± 1.8)x10-10
  S2: (5.0 ± 1.3)x10-11
Fallout rate increased by two to three orders of magnitude

## Slide 11
Conclusions
The ICP-MS based method as an effective tool to inform dust backgrounds and evaluate mitigation procedures
Next steps
Leverage the method to develop quantitative material cleaning procedures
Develop methods to directly determine contribution to dust backgrounds from 238U progeny (e.g., 210Pb)
The efficacy of mitigation procedures in place at SNOLAB
Dust backgrounds in clean laboratories are strongly affected by ongoing activities and handled materials
This study demonstrated:
Note:
The method is being used within the SuperCDMS collaboration to monitor backgrounds from dust fallout during installation activities.

## Slide 12
DOE, USA Office of High Energy Physics Advanced Technology R&D subprogram (KA-25)
Canada Foundation for Innovation
Province of Ontario Ministry of Research and Innovation

## Slide 13
Backup slides

## Slide 14
Triple quadrupole ICP-MS (ICP-QQQ-MS), or tandem ICP-MS (ICP-MS/MS)

## Slide 15
Method validation
*
*
*
*
*
*
*
*Upper limits
Same locations
Same exposure time
ICP-MS vs XRF measurement of Ca and Fe fallout rate (2018 sample collection)