## Slide 1: A Case for Iridium-Platinum: an ultrasensitive bilayer Transition Edge Sensor
Maggie Reed: On behalf of the TESSERACT Collaboration
Nov. 8th: RDC7 CPAD 2023

## Slide 2: Motivation
Aka who cares?

## Slide 3
Overview: TES Design Choices
Design options: Build-A-TES
Material
Method of Tc Control
Thermal isolation
Multilayers, magnetically doped SC, elemental SC
Superconducting, low transition temperature
micro structures, phonon decoupling (acoustic mismatch, hot electron effect)
Absorber
Radiation type dependent
Notes: Heat capacity of absorber should be small compared to the TES (extra heat capacity decreases sensitivity and increases noise). Controlling thermal conductance (G).

## Slide 4
Overview: Calorimeter Model and Design Choices
Sensor
Absorber
Thermal Bath
Method of Tc Control
Thermal isolation
Absorber
Your choices will impact this system heavily, and will be made depending on your purpose! In our case….
Notes: Our system relies on making choices which efficiently thermalize the input energy, measure the change from that energy, while also isolating how we measure thermally.

## Slide 5
Motivation: a Single Photon Device
If we wanted to make a single photon device, we would need:
  High quantum efficiency
  Excellent energy resolution
  Fast response time
  Low background rates
Traditionally, Tungsten has been the thin film choice* in the past, given the above requirements
Quantum information, rare event searches, astroparticle experiments…
For good reason! (hot electron effect[3], low background rate….)
So why focus on anything else?
Notes: *W TES’s can act as the actual absorber material directly, or as a secondary absorber (like in QET’s). Hot electron effect: electrons and phonons at two different temperatures. Electron temp is not in equilibrium with phonons. Enhanced in W.

## Slide 6
Motivation: W Film Limitations (why we care!)
Tc precision and variability
  Mixed phase is needed to get Tc in desired range
  Sensitive to fabrication parameters
High electrical resistivities
  For single photon applications, we want fast energy spread!
Noise: bare TES have Low Energy (<200eV) Excess (LEE) noise[1].
LEE Noise:
Seen in W films (stress?)
See R. Romani RDC7+8 Thurs 4PM
Notes: *high resistivity mean small thermal conductivities mean thermal energy from a single photon must spread in a time much less than thermal time constant. This limits your detector speed and area.

## Slide 7: On Iridium Platinum

## Slide 8
An Iridium-Platinum Bilayer Device: Why Ir-Pt?
Ir-Pt Bilayer:
  Tuneable Tc (proximity effect)
  Reproducibility
  Tc suppression:
High performance (as we will see!), hits requirements for single photon applications
Already beginning to be more widely used
[2] G. Wang et al. (2017)
Notes: Multilayer systems: superconductor + normal metal composite. Layers are thinner than the SC coherence length, composite film has reduced Tc compared with the SC film

## Slide 9: Performance and Results
Can we achieve competitive single photon detectors with excellent energy resolution using IrPt? (Spoiler: Yes!)

## Slide 10
Setup
Two devices of different sizes on single wafer (Correlated noise studies!)
  Fab at Argonne National Laboratory[5] (see: initial thermal studies at ANL)
  Tc tuned at 74-76 mK
Device characterization at UC Berkeley Pyle Lab in a CryoConcept fridge at base 6mK
Big and small devices

## Slide 11
Device Characteristics: Quick and Dirty Overview
For a more in depth breakdown of our characterization flow see my poster from LTD20!
DC Characteristics
ITES v Ibias for static parameters. Helps us build the next step.
AC Characteristics
dIdV: device response to an impulse. Builds the template we will use to do Optimum Filtering (OF)
Noise Modeling
Preliminary estimate of energy resolution + backgrounds (start getting excited)
Feature extraction from OF, analysis
Energy resolution of devices from continuous random data!

## Slide 12
IrPt Bilayer: Energy Thresholds
The big cheese: energy baseline resolution from randoms (4𝞼 trigger)
𝞼E= 73 meV

## Slide 13
IrPt Bilayer: sub-eV threshold
Sub-eV baseline energy resolution in context
W and Ti are not the only ways to make competitive single photon sensitive devices
  LEE fundamentally limits us below 200 eV
  Alternatives should be explored!
Relative performance of single photon TES’s
TES | Tc (mK) | VTES(um3) | 𝛔E(meV)
Ti | 50 | 0.13 | 47
TiAu | 106 | 90 | 48
MoCu | 110 | 2000 | 295
W | 125 | 22 | 120
IrPt | 74 | 7500 | 73 (preliminary)
[4] C.W. Fink et al. (2020)
Notes: With volume correction: sigma_E / Sqrt(V_TES). C and G depend linearly on TES volume. Sigma_E ^2 goes as Volume*Tc^3 in the non athermal case (Tc is higher in the athermal case since minimization occurs when phonons bounce for a long time). Heat capacity and volume are proportional in normal metals and entirely due to electrons. SC has both phonon and electrical contributions but generally at Tc heat capacity is like 2 times the normal metal value. C is actually measured by complex impedance.

## Slide 14: Mysteries in the Data
Fantastic energy resolution! But…
Courtesy of NASA, ESA, CSA, J. DePasquale: The James Webb ? galactic merger

## Slide 15
Big IrPt TES: Issues
Energy threshold of big TES was only 355 meV
  Means we can’t properly analyze events across both devices (recall our amazing 73 meV small TES threshold)
Excess broadband noise
Current noise for the big device at the bias point
Current Noise [A/√Hz]
Frequency [Hz]

## Slide 16
Unknown “Blob” on Small Device
Can’t check if coincident (big TES threshold too high)
Further analysis confirms these are real events (random in time, normal pulse shape)
Not from stress: single energy, not a continuum
So…. what is it?
Randoms
Threshold
Weird blob
Big v Small Device Energies
[meV]
Small TES energy [meV]
Big TES energy [meV]

## Slide 17
Blob Possibilities
IR leak
Poisoning from FR4 board scintillation internal to the device housing
Something else?
These are both solved now after our most recent hardware upgrades!

## Slide 18: Final Thoughts

## Slide 19
Food for Thought
Bilayer IrPt TES devices are promising low-energy devices with excellent energy thresholds (𝞼E= 73 meV )
Recent hardware improvements at our UC Berkeley Lab motivate our intentions to do a Dark Matter search with these devices! (At even lower TC)
Stress problems (LEE) encourage device ingenuity and forays into new materials and methods
Further study is needed to investigate!
We do not have to stick with W!
Potential new backgrounds? (Blob)

## Slide 20: Thank You!
Visit us at: https://tesseract.lbl.gov/
TESSERACT

## Slide 21
References
[1]Adari, Prakruth et al. “EXCESS workshop: Descriptions of rising low-energy spectra.” (2022).
[2]G. Wang et al., "Modeling Iridium-Based Trilayer and Bilayer Transition-Edge Sensors," in IEEE Transactions on Applied Superconductivity, vol. 27, no. 4, pp. 1-5, June 2017, Art no. 2100405, doi: 10.1109/TASC.2016.2646373.
[3]Irwin, Kent D. and G. C. Hilton. “Transition-Edge Sensors.” (2005).
[4]Fink, C. etal., Characterizing TES power noise for future single optical-phonon and infrared-photon detectors. AIP Advances. 10. 085221. 10.1063/5.0011130. (2020).
[5]Zhang, J., Chang, C.L., Fujikawa, B. et al. Characterization of the Thermal Properties of Ir/Pt Bilayer Transition Edge Sensors. J Low Temp Phys 210, 194–208 (2023)

## Slide 22
Small TES

## Slide 23
Small TES

## Slide 24
Small TES

## Slide 25
Small TES blob population time since last event

## Slide 26
Small TES blob population actual traces