## Slide 1: STA Skipper and CCD Development Status
Image Sensors for Precision Astronomy
SLAC
12 March, 2024
Greg Bredthauer, Kasey Boggs, Joe Tufts
greg.bredthauer@sta-inc.net
http://www.sta-inc.net

## Slide 2: STA
Richard Bredthauer, 1975: “A 50-bit charge coupled device with AC coupled inputs”
Hubble WFPC2
Mars Pathfinder Stereo Imager
All Cassini CCDs
STA founded 1999

## Slide 3: Custom Sensors: PACE OCI UVNIR
Launched February 7, 2024
Ocean monitoring (Plankton, Aerosol, Cloud ocean Ecosystem; Ocean Color Instrument)
512 x 128 26um TDI, 16 outputs
Red and Blue tuned AR, 310-610nm, 595-895nm, custom conversion gains across sensor
See OCI Flight UVNIR CCD Procurement Specification; Falcon 9 photo from NASA/SpaceX

## Slide 4: Custom Controllers
HxRG: ADM, 18 channel 18-bit 12.5MHz modules  72 channels per controller
BOSS spectrograph upgrade: one Archon synchronously reading out an LBNL 3-phase deep depletion p-channel 4k x 4k CCD and an e2v 4-phase n-channel 4k x 4k CCD231-84

## Slide 5: Microchip Foundry
200mm wafers (150mm at Teledyne DALSA)
5x stepper masks instead of 1x masks
 Immediately attempted an 8k x 8k 15um CCD
Stitching boundaries  ~0.3% feature in PRNU

## Slide 6: STA5100
First cold testing of BSI STA sensor from Microchip foundry, thinning done at ITL
Same format as STA4850, 4 single stage outputs, 4080 x 4080 15um, 1000ohm-cm 30um epi

## Slide 7: STA5100
4uV/e-, 2.7e- RMS at 100kHz, 4e-/pixel/hour at -100C, 200ke- full well

## Slide 8: Prototype Skipper Device
1k x 2k frame transfer, 12um pixels
1 standard single stage output, 1 skipper output

## Slide 9: Skipper Test Results
Cooled to -100C
Skipper gain 2.5uV/e-
5.5e- single sample noise at 100kHz
5.06e- flat field
0.19e- noise (2000x sampling)
 Perfect gain and linearity, no PTC needed

## Slide 10: LBNL STA5500
Design goal: Blue-sensitive 4k x 4k CCD with < 1e- read noise and a readout time < 60 seconds.
Prototype skipper output modified to reduce capacitance, single sample noise should go from 5.5e-  4e-
128 outputs total; 32 series skipper outputs per quadrant 4e- / sqrt(32)  ~0.7e- using 100kHz readout (10us per sample)

## Slide 11: LBNL STA5500

## Slide 12: Differential Skippers

## Slide 13: MOSFET Tuning
Want to optimize the output to minimize the read noise, so fewer skipper cycles are needed to get to the noise goal
Experimented with an STA4800 prototype with 16 output design variants (transistor W/L, supernotch, buried contacts, etc), programmable current loads
 We’re already at the optimal MOSFET geometry

## Slide 14: JFET Design
MIT/LL has reported JFET outputs with ~1e- read noise at 100kHz
Silvaco 3D simulation used to develop a JFET output design
Simulation work supported in part through a collaboration with Prof. Hamden at the University of Arizona

## Slide 15: JFET Design
The JFET design shown is predicted to have 0.1fF gate capacitance, 1k output impedance with a 1.8mA drain current, and a source follower gain of 0.9998
Drain
Gate
Source
Source
Guard

## Slide 16: JFET Structure

## Slide 17: JFET Operation

## Slide 18: JFET vs MOSFET
Prototype skipper: 20x4 floating gate  20fF, MOSFET  15fF 0.7 x q/(20fF + 15fF) = 3.2uV/e- (2.5uV/e- measured)
Skipper with JFET: 12x4 floating gate  12fF 0.99 x q/(12fF) = 13.2uV/e-
 Time to build something new, results later this year