## Slide 1: REBCO High-Temperature Superconductor Coatings for RF Applications
Sergio Calatroni, on behalf of the Collaboration.

## Slide 2: Setting the scene: future accelerators

## Slide 3
Work supported by the European Commission under the HORIZON 2020 projects EuroCirCol, grant agreement 654305; EASITrain, grant agreement no. 764879; iFAST, grant agreement 101004730, FCCIS, grant agreement 951754; E-JADE, contract no. 645479; EAJADE, contract number 101086276; and by the Swiss CHART program
http://cern.ch/fcc
Future Circular Collider

## Slide 4: FCC integrated program
FCC-ee
2020 - 2040
2045 - 2063
2070 - 2095
FCC-hh
comprehensive long-term program maximizing physics opportunities
stage 1: FCC-ee (Z, W, H, ) as Higgs factory, electroweak & top factory at highest luminosities
stage 2: FCC-hh (~100 TeV) as natural continuation at energy frontier, pp & AA collisions; e-h option
highly synergetic and complementary programme boosting the physics reach of both colliders (e.g. model-independent measurements of the Higgs couplings at FCC-hh thanks to input from FCC-ee; and FCC-hh as “energy upgrade” of FCC-ee)
common civil engineering and technical infrastructures, building on and reusing CERN’s existing infrastructure
FCC integrated project allows the start of a new, major facility at CERN within a few years of the end of HL-LHC
Link to the FCC week 2024
From M. Benedikt, FCC Study leader

## Slide 5: The Compact Linear Collider (CLIC)
  Timeline: Electron-positron linear collider at CERN for the era beyond HL-LHC
  Compact: Novel and unique two-beam accelerating technique with high-gradient room temperature RF cavities (~20’500 structures at 380 GeV), ~11km in its initial phase
  Expandable: Staged programme with collision energies from 380 GeV (Higgs/top) up to 3 TeV (Energy Frontier)
  CDR in 2012 with focus on 3 TeV. Updated project overview documents in 2018 (Project Implementation Plan) with focus 380 GeV for Higgs and top.
Accelerating structure prototype for CLIC: 12 GHz (L~25 cm)
The CLIC accelerator studies are mature:
Optimised design for cost and power
Many tests in CTF3, FELs, light-sources and test-stands
Technical developments of “all” key elements
  Recent talks: eeFACT-I1 and eeFACTI2
From: Steinar Stapnes

## Slide 6: The ILC250 accelerator facility
e- Source
e+ Main Liinac
e+ Source
e- Main Linac
Damping Ring
Beam dump
Interaction point
Physics Detectors
Bunches of ~1010 e+/e-
Creating particles Sources
  polarized elections/positrons
High quality beam Damping ring
  low emittance beams
Acceleration Main linac
  superconducting radio frequency (SRF)
Collide them Final focus
  nano-meter beams
Go to Beam dumps
Undulator positron source
Electron driven positron source
  Recent talks: eeFACT-I1 and eeFACTI2
From: Steinar Stapnes

## Slide 7: From JoAnne Hewett, FCC week 2024

## Slide 8: Power and energy: LHC and future machines
Very uncertain but MTP assumes 120 MCHF/TWh beyond 2026.
With “standard” running scenario (on the right) every 100 MW corresponds to ~0.6 TWh annually, corresponding to ~75 MCHF annually.
From: Steinar Stapnes
Linear collider studies predict roughly similar power consumption for equivalent machines (ILC vs CLIC)
Obsolete

## Slide 9: How can SC and NC have the same power consumption?
Linear collider RF systems fall in two categories
Despite the ~106 difference in quality factor, (~103 considering cryo efficiency), pulsing at low duty factor allows reducing the average consumption for NC accelerating structures down to the SC level – which cannot be effectively be pulsed
In our study, we want ultimately to verify whether HTS in pulsed RF mode allows a further power gain compared to both Nb and Cu
SC niobium, Q01010, 35 MV/m, CW
NC copper, Q0104, 100 MV/m, pulsed

## Slide 10: C3, a new kid on the block?
More info on C3 here
From: Emilio Nanni
Even a factor 10 improvement in Q factor compared to copper
could pave the way for energy savings

## Slide 11: High-temperature Superconductors

## Slide 12: Superconductors zoo
By PJRay - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=46193149

## Slide 13: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Jc may vary of orders of magnitude.
Hc2 has much smaller variation.
YBCO most promising candidate
NbTi – NbTiN possible candidates at B < 10T
Nb3Sn for B < 15 T

## Slide 14: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Pinning force

## Slide 15: REBCO coated conductors
REBCO crystal structure
Charge transport in planes
High anisotropy
Extreme sensitivity to oxygen content
Large and small
Electronic features:
Scheme of Coated Conductor (CC)
Buffer layers allow biaxial epitaxial REBCO growth
Metallic substrate makes tape ductile
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 16: Type II superconductors
Magnetic phase diagram
for type II SC
Vortex length scales:
Distance upon which magnetic field decays.
Distance upon which the order parameter decays.
Vortex in type II SC
Characterized by mixed phase
with vortex penetration.
Abrikosov lattice
Distribution into hexagonal lattice in homogenous material.
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 17: Vortex pinning
Defects: Strategy to pin vortices
Lorentz-like force provokes vortex movement
Defect landscape:
0D: Impurity atoms, interchanged atoms
1D: Dislocations, columnar defects
2D: Twin boundaries, grain boundaries
3D: Nanoparticles, associated strained regions
Critical current density
The maximum value of without moving the lattice, without presenting resistance.
Scales with current density and magnetic field
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 18: Various producers of CCs
CCs differ in architecture and REBCO microstructure.
YBCO (1.6 ) + BZO nanorods
EuBCO (2.5 ) + BHO nanorods
GdBCO (1.5 )
YBCO (3 ) + Y2O3 nanodots
Bruker
Fujikura APC
SuNAM
SuperOx 2
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 19: HTS coating technologies
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 20: Outline
The past (?): HTS at low RF gradient, in a strong magnetic field
  FCC beam screens and RADES axion detectors
The present: HTS at high-gradient RF
  The I.FAST collaboration CERN – KIT – ICMAB, with the support of SLAC
The future (???): HTS in both high-gradient RF and strong magnetic field
  The muon collider

## Slide 21: Outline
The past (?): HTS at low RF gradient, in a strong magnetic field
  FCC beam screens and RADES axion detectors
The present: HTS at high-gradient RF
  The I.FAST collaboration CERN – KIT – ICMAB, with the support of SLAC
The future (???): HTS in both high-gradient RF and strong magnetic field
  The muon collider

## Slide 22: HTS for the FCC-hh beam screen
FCC-hh, a proposed 100 TeV p-p collider at CERN, with 16 T dipoles operated at 1.9 K
A beam screen held at 50 K, to protect the dipoles from synchrotron radiation ~30 W/m/beam (LHC < 0.2 W/m)
HTS materials instead of copper in the FCC-hh beam screen, to improve beam stability (-> impedance) at 50 K
Bunched particle beams produces RF fields, up to ~1 GHz
Extremely challenging requirements:
  HTS must operate at 50 K and 16 T
  Critical fields Hc2 , Hirr >> 16T
  Jc > 25 kA/cm2 (2.5x108 A/m2)
  Surface resistance Rs better than for copper
Compatible with accelerator environment
  Minimize dipole field distortion due to persistent currents
  UHV compatible, low SEY, lifecycle assessment, etc..
16 Tesla !
Calatroni, IEEE TAS 26, 3500204 (2016)
Calatroni et al, SuST 30, 075002 (2017)

## Slide 23: Two material choices
Coat the inside of the screen
with Tl-1223 films
Manufacture the screen using REBCO tapes soldered to the screen

## Slide 24: RF when an external magnetic field is present
Vortex pinning
  Artificial pinning centres
Vortex lattice
  cylindrical normal conducting regions tens of nm diameter
  Each vortex carries one flux quantum
Apply RF Current
  Motion of vortices  dissipation
    The motion of the rigid vortex lattice behaves as an harmonic damped oscillator with quadratic potential
Simplified model valid for estimates and scaling
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506
Coffey, Clem PRL 67, 386 (1991)
Brandt PRL 67 2219 (1991)
Silva et al, PRB 78, 094503 (2008)
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 25: Validation of RF performance (UPC - ICMAB)
In house developed 8.05 GHz cavity resonator compatible with 25mm bore 9 T magnet at ICMAB
REBCO CCs outperform Cu at 50K and up to 9T
RS is microstructure dependent
Puig et al, SuST 32, 094006 (2019)
Surface currents equivalent to 0.1 MV/m of a typical accelerating cavity

## Slide 26: Coating process I
2) Edge removal
1) Pre-tinning
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Developed in the context of FCC-hh impedance reduction by coating the beam screen with HTS tapes

## Slide 27: Coating process II
3) Soldering
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
4) Substrate extraction
Solder
Cu
Ag
REBCO
Cu
Surface to coat
Cu
Substrate
Buffer layers
Ag
Cu
Solder
Cu
Ag
REBCO
Substrate
Buffer layers
Ag
Cu
Surface to coat
Cu
N. Lamas et al., to be published

## Slide 28: Development of soldering technology
CC
Solder
Beamscreen
HTS tapes
Solders based on Sn / Pb / Cu / Bi & In temperatures < 220ºC
2x80 km of beam screens to be coated with HTS

## Slide 29: HTS for axion searches
Increase Q
copper coating  superconducting coating
Requirement: High quality factor in a high magnetic field
Motivation:
Axion haloscope

## Slide 30: First real cavity, f9 GHz
We have developed a technology for applying 2D HTS tapes to 3D RF “RADES” cavities demonstrating the potential of HTS for RF applications J. Golm et al., IEEE TAS, Vol. 32, No. 4, (2022) 1500605
2x improvement of RF quality factor compared to copper
(newer prototype 5x improvement)
RADES cavity for axion searches
12 mm-wide HTS tapes

## Slide 31: First published physics results with an HTS coated cavity
arXiv:2403.07790

## Slide 32: Other results from CAPP
From: D. Ahn, CAPP. More info at Patras Workshop
2.2x10-5 
3.5x10-5 

## Slide 33: Outline
The past (?): HTS at low RF gradient, in a strong magnetic field
  FCC beam screens and RADES axion detectors
The present: HTS at high-gradient RF
  The I.FAST collaboration CERN – KIT – ICMAB, with the support of SLAC
The future (???): HTS in both high-gradient RF and strong magnetic field
  The muon collider

## Slide 34: First: a caveat
Bulk Nb
HiPIMS +DC Bias
Nb/Cu samples
HIE-ISOLDE
JC decrease is guiding the development of Nb/Cu films
Rationale:
Results from HIE-ISOLDE and bulk Nb
Modelling of losses as hysteretic losses from RF fluxons penetration
Existing HTS Coated Conductors might not be the best choice at high-gradient RF, being optimized for flux pinning
4K, 250mT
From: Carlota Pereira Carlos

## Slide 35: Low-power RF measurements
An improvement larger than x10 compared to copper (Rs=8m) has been measured on samples of tapes (8 GHz) at low RF power
Adapted from Romanov et al, Sci. Rep. (2020) 10:12325
Cu

## Slide 36: Testing at higher RF power
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022
THEVA inclined deposition
0 T external field
HTS coated conductors at 8 GHz (dielectric resonator) and 50 K

## Slide 37: Literature review
There are very few measurements on HTS at high RF currents (mostly microstrip resonators). But physics is proven.
~1011 A/m2 RF current (microstrip resonator, 200 µm, 350 nm thick, 8 GHz)
Powell et al. Journal of Applied Physics 86, 2137 (1999)
For 1 µm thickness this is equivalent to 105 A/m ( 0.1 T  25 MV/m)
Entering the “high-gradient” range

## Slide 38: High-gradient testing at SLAC – supported by I.FAST IIF
“Mushroom” cavity. Can achieve Hpeak of about 360 mT – 2.9x105 A/m (equivalent to ~80 MV/m in a standard accelerating cavity) using 50 MW XL-4 Klystron at 11.4 GHz.
Zero E-field on the sample
Maximum H-field on the sample
Sample accounts for ⅓ of total cavity loss
Goal: demonstrate high-gradient pulsed operation of HTS, at cryo-temperatures

## Slide 39: First results at SLAC, at low gradient
Two HTS measurements, after calibration measurements with Cu and Nb
Rs Cu  17 m
Rs REBCO tapes  1.7 m
Rs REBCO PVD  1.0 m
Directly grown REBCO on MgO and on copper+MgO (CERACO)
Soldered REBCO-CCs on copper (Fujikura by CSIC-ICMAB)

## Slide 40: Preliminary SLAC results at high-gradient I
From: Mitch Schneider

## Slide 41: Preliminary SLAC results at high-gradient II
From: Ankur Dhar
Shaded area: change from 100 W to 1.6 kW of forward power

## Slide 42: First device validation – supported by I.FAST Innovation Fund
Next goals: develop large-size tapes (50 mm wide) in collaboration with KCT, to be first tested on discs at SLAC. Two-years plan funded by IIF
(Ideally: REBCO coating directly on 3D objects)
Device validation: X-band pulse compressor (SLAC) as first “real” RF device
Coating will be performed by CSIC-ICMAB
Courtesy Greg LeSage, SLAC
Pulse compressor

## Slide 43: Axion cavity as earlier demonstrator
Approach being validated also for axion detection cavities in RADES collaboration having a similar geometry
Copper body manufactured at Mainz University, adapted to 12 mm wide coated conductors, coated by CSIC-ICMAB
Axion cavity
Q0 = 268 520 (75%)
    Surface currents
    E-field
    f= 9.3 GHz
Q0 = 356 070

## Slide 44
Summary of milestones and deliverables: WP1 CERN
M1 - Samples and substrates procurement (due 12/2023). Achieved but we have some alignment difficulties of the segments still to be solved
D1 - RF low power characterization of segmented cavities (small tapes) (due 6/2024). On track with some potential small delays pending the solution of the above difficulties. However, this is mitigated by:
Extra – Segmented cavity from SLAC already produced (was foreseen after completion of HIGHEST) and commissioned ready to be coated with small tapes
CERN
SLAC confidential
Do not disclose
Segmented cavity
Segmented cavity

## Slide 45
Summary of milestones and deliverables: WP2 KCT
M1 - Design and fabrication of sample holder system (due 3/2024). Achieved well in advance
D1 - HTS coating of large samples (due 3/2025). On track and well under way, first 40 mm wide tape already coated (final goal is 50 mm, but 40 mm is enough for our final goal)
KCT confidential
Do not disclose
Roll to roll coater for HTS tapes
40 mm wide HTS tape

## Slide 46
Summary of milestones and deliverables: WP3 CSIC
D1 - Coating on discs and segmented cavities for benchmarking (small tapes) (due 3/2024). Achieved for discs, already high-power tested at SLAC (presented at EUCAS 2023 / IPAC 2024) waiting for readiness of segmented cavity
D2 - Measurement of superconducting properties of large size tapes (due 3/2025). On track and well under way, first 40 mm wide tape already characterized
CSIC confidential
Preliminary results
Do not disclose
Copper disc coated with 12 mm tapes
First tests of 40 mm tape